Zuidgeest, Lonneke

Characterization of biopolymer networks in k-carrageenan gel using nanoprobe diffusometry

Graduation project 			Date: 26-05-2016

Lonneke Zuidgeest 			s1078336

Unilever R&D Vlaardingen		Department Imaging & spectroscopy

Wageningen University			Laboratory of Biophysics

Hogeschool Leiden			Internship period 	01-12-2015

02-06-2016

- Bachelor thesis:

- Characterization of biopolymer networks in k-carrageenan gel using nanoprobe diffusometry

Author/ student:
Name:			Lonneke Zuidgeest
Student number:	1078336

Placement Company:

Name:			Wageningen University

Address:		Dreijenlaan 3

Building 312 (Transitorium)

6703 HA Wageningen

Department:		Laboratory of Biophysics

Supervisor:		Dr. Johannes Hohlbein

Signature supervisor:

Name:			Unilever R&D Vlaardingen

Address:		Oliver van Noortlaan 22

3133 AT Vlaardingen

Department:		Imaging & Spectroscopy

Supervisor:		Prof. Dr. John van Duynhoven

Signature supervisor:

Educational Institution:

Name:			Hogeschool Leiden

Address:		Zernikedreef 11

2333 CK Leiden

Department:		Applied Science

Study:			Chemistry

Track:	 		Analytical chemistry

Supervisor:		Pieter de Koe

Internship period:	01-12-2015 - 02-06-2016

Date:			15-03-2016

Project:

Name:			NWO-TA-COAST1 DINAMISCH

Diffusional Nanoprobes for MultI-length Scale material Characterization

Collaboration:		NWO

COAST

Unilever

Wageningen University

# Samenvatting

Het biopolymeer netwerk bepaalt de macroscopische eigenschappen in voeding zoals smaak, mondgevoel en opnamen/uitgiften eigenschappen. De structuur van het biopolymeer netwerk verschilt op meso schaal (mm tot nm). Κ-carrageen gel werd geselecteerd als een model systemen, omdat deze polysacharide in aanwezigheid van kationen een gecontroleerde biopolymeer structuur heeft. Het doel van dit onderzoek was de karakterisatie van het biopolymeer netwerk in κ-carrageen gels met nanoprobes diffusometrie. Eerst werd het biopolymeer netwerk van de κ-carrageen gel in beeld gebracht met transmissie elektron microscopie (TEM), vervolgens werd de nanoprobe diffusie gevold met fluorescentie recovery na (after) foto bleken (photobleaching), FRAP en single particle tracking (SPT) met totale interne reflectie microscopie (TIRFM). Er werden vijf 2 % (m/m) κ-carrageen gels met 20 mM KCl en 0, 50, 100, 150 en 200 mM NaCl gemaakt. De biopolymeer netwerken van de κ-carrageen gels werden afgebeeld met tweedimensionaal (2D) en driedimensionaal (3D) TEM. 2D TEM toonde een heterogeen en dicht en grof netwerk voor de 0 mM NaCl κ-carrageen gel. Voor κ-carrageen gels met 50, 100, 150 en 200 mM NaCl de netwerken waren homogeen en grof. Door gebrek aan contrast werd met 3D TEM reconstructies alleen groffen netwerken in beeld gebracht. De TEM methodes zijn tijdrovend, kunnen het netwerk verstoren en zijn slechts een moment opname. Nanoprobe diffusometrie is een kwantitatieve methode die de diffusie van nanoparticles volgt voor de karakterisatie van een netwerk. Nanoprobe diffusometrie kan gebruikt worden als alternatief voor TEM. FRAP experimenten werden uitgevoerd op een confocale laser scanning microscoop (CLSM). Een geïmmobiliseerde fractie nanoprobes in de κ-carrageen gels werd berekend met de verkregen FRAP curven. Een grote immobiele fractie nanoprobes in de κ-carrageen gels met ≤ 100 mM NaCl duidde op een dicht netwerk met gevangen nanoprobes. De κ-carrageen gels met > 100 mM NaCl hadden een kleinere immobiliën fractie, dus een groffer netwerk. De heterogeniteit op micron schaal in de κ-carrageen gels met 0 mM en 50 mM NaCl kon worden vast gelegd met CLSM afbeeldingen van gewassen gels. Losse vrij diffunderende deeltjes en gevangen deeltjes konden worden gevolgd met TIRFM-SPT. Verdere optimalisatie van de TIRFM-SPT methode is echter nodig voor de karakterisatie van het biopolymeer netwerk in κ-carrageen gel. Nanoprobe diffusometrie is een snelle en kwantitatieve methode voor de karakterisatie van het biopolymeer netwerk in κ-carrageen gel.

# Abstract

Biopolymer networks determine the macroscopic properties of many food materials such as taste, mouthfeel, controlled release, delivery characteristics and barrier properties. The structure of these networks consists of details on various length scales ranging from nano- to millimetres. We selected κ-carrageenan gel as a model system since this polysaccharide is widely used in the food industry as thickener. The main objective is the characterization of the biopolymer networks of κ-carrageenan gel with nanoprobe diffusometry. First, the biopolymer networks in κ-carrageenan gel was visualized with transmission electron microscopy (TEM) and next nanoprobe self-diffusion was monitored with fluorescence recovery after photo bleaching (FRAP) experiments and single particle tracking (SPT) on a total internal reflection microscope (TIRFM). Five 2 wt% κ-carrageenan gels with different sodium chloride concentrations (0 mM, 50 mM, 100 mM, 150 mM and 200 mM NaCl) and constant potassium chloride (20 mM KCl) were made. The biopolymer networks of the κ-carrageenan gels were visualized with two-dimensional (2D) and three-dimensional (3D) TEM. 2D TEM showed heterogeneous and dense networks for a 0 mM NaCl κ-carrageenan gel and coarse, homogeneous networks for 50, 100, 150 and 200 mM NaCl κ-carrageenan gels. 3D TEM reconstructions showed only the coarse networks in the κ-carrageenan gels. TEM techniques are invasive, thereby potentially perturbing the network, time consuming and provides only static snapshots of the structure. To overcome these limitations, a different approach was applied which monitors the diffusional behavior of nanoprobes in the networks to characterize and quantify structural properties. Fluorescence recovery after photo bleaching (FRAP) experiments were performed with a confocal laser scanning microscope (CLSM). With the obtained FRAP curves an immobile fraction of nanoprobes could be identified. The large immobile fraction of nanoprobes in the κ-carrageenan gels formed with ≤ 100 mM NaCl indicated a dense networks in which nanoprobes got trapped. The κ-carrageenan gels wit > 100 mM NaCl had a smaller immobile fraction of nanoprobes indicating coarser networks. The micron scale heterogeneity in the κ-carrageenan gels with 0 mM and 50 mM NaCl could be imaged by performing CLSM on washed gels. Single particle self-diffusion could be followed and trapped nanoparticles were imaged with TIRFM-SPT. No quantification could be provided due to sub-optimal concentration of the nanoprobes in the κ-carrageenan gels. Overall, the results showed that nanoprobes diffusometry can be used for quantitative characterization of biopolymer network heterogeneity in κ-carrageenan gels.

# Contents

Samenvatting	2

Abstract	3

Contents	4

Abbreviations	5

1.	Introduction	6

2.	Theory	7

Carrageenan gels	7

Transmission electron microscopy	8

Nanoprobe diffusometry	10

CLSM-FRAP	11

TIRFM and single particle tracking	13

Preparation of k-carrageenan gels	15

TEM characterization of κ-carrageenan gels	15

CLSM-FRAP	16

FRAP data analysis	17

CLSM images trapped fraction	18

TIRFM single particle tracking of QD’s in κ-carrageenan gels	19

4.	Results and discussion	21

TEM characterization of κ-carrageenan gels	21

CLSM-FRAP assessment of G5-ATTO dendrimer diffusing in κ-carrageenan gels	24

CLSM characterizing trapped G5-ATTO dendrimer in washed κ-carrageenan gels	29

TIRFM single particle tracking of QD’s in κ-carrageenan gels	31

Overall discussion	36

5.	Conclusions	38

6.	Recommendations	38

7.	Acknowledgment	39

8.	Bibliography	40

Appendix A. Method Embedding	41

Appendix B. Method Ultramicrotomy	42

Appendix C. 2D TEM magnification 62000 x	45

Appendix D. FRAP data	46

Appendix E. Background FRAP	48

Appendix F. Average corrected and normalized FRAP curves	49

Appendix G. CLSM images of trapped fraction	51

Appendix H. Plan of approach	52

# Abbreviations

2D:		Two-Dimensional

3D: 		Three-Dimensional

CLSM: 	Confocal Laser Scanning Microscopy

COAST:	Comprehensive Analytical Science and Technology

CPD:		Cumulative Probability Distribution

DINAMISCH:	Diffusional Nanoprobes for MultI-length Scale material Characterisation

FCS:		Fluorescence Correlation Spectroscopy

FRAP: 		Fluorescence Recovery After Photobleaching

MSD:		Mean Square Displacement

MSDS:		Materials Safety Data Sheet

NMR:		Nuclear Magnetic Resonance

NWO:		Nederlandse Organisatie voor Wetenschappelijk Onderzoek 
Netherlands Organisation for Scientific Research

PEG:	Polyethylene glycol

QD:	Quantum Dot

SEM:		Scanning Electron Microscopy

SPT:		Single-Particle Tracking

TEM: 		Transmission Electron Microscopy

TIRF:		Total Internal Reflection Fluorescence

TIRFM:	Total Internal Reflection Fluorescence Microscopy

# Introduction

Macroscopic properties of many food materials are determine by their biopolymer networks in particular taste, mouthfeel, controlled release, delivery characteristics and barrier properties. The structure of biopolymer networks comprises features on various length scales ranging from nano- to millimetres. Κ-carrageenan gel was selected as a model system, this polysaccharide is widely used in the food industry as thickener, stabilizer and gelling agent. Cations have a big influence on the gelation of the biopolymer network of κ-carrageenan gel (Hermansson, 1991). The microstructure of κ-carrageenan gels can therefore be controlled by the cation concentration. The biopolymer networks can be visualized by transmission electron microscopy (TEM). This technique is however invasive, potentially perturbing the network, time consuming and provides only static snapshots of the structure. To overcome these limitations, an emerging approach can be applied which measures the diffusional behavior of nanoprobes in order to characterize and quantify structural properties of biopolymer networks. An exising approach is to use confocal laser scanning microscope (CLSM) in combination with assessment of fluorescence recovery after photobleaching (FRAP) on fluorescent nanoprobes. Until now FRAP has been mainly used to research the dynamics of molecules in living cells, membranes and other biological systems. A promising, but not yet widely applied method for nanoprobe diffusometry is single-particle tracking (SPT) on a total internal reflection fluorescence microscopy (TIRFM). This method is able to follow the self-diffusion of single particles. Both FRAP and TIRFM-SPT have the advantage that they are quick and non-invasive and thus hold the promise to improve the understanding of biopolymer networks in a wide range of food materials.

The main objective is the characterization of the biopolymer networks of κ-carrageenan gel with nanoprobe diffusometry. This objective is divided into three secondary objectives.

- Characterization of biopolymer networks of κ-carrageenan gel with TEM in 2D and 3D

- Establish feasibility of biopolymer network characterization of κ-carrageenan gels with CLSM-FRAP

- Establish feasibility of biopolymer network characterization of κ-carrageenan gels with TIRFM-SPT

# Theory

## Carrageenan gels

Carrageenan is a polysaccharide extracted from seaweeds and specially the red algae (also called Rhodophyceae) which, uses carrageenan as cell-wall material. Carrageenan is a general name for a family of viscosifying or gel forming biopolymers. Since the 15th century carrageenan has been used as a thickener, stabilizer and gelling agent in food. Current products containing carrageenan are, for example, chocolate milk, (frozen) yoghurt, whipped cream, jellies, sauces and frozen desserts. Carrageenan is also used in pharmacy and cosmetics. Carrageenan is a biopolymer with a backbone of a mixture of sulfated D-galactose. There are three carrageenans, identified by the Greek letter kappa (κ), lambda (λ) and iota (ι), that are most common used for food products. Only kappa and iota carrageenan can form a gel structure, because these polysaccharides have a 3,6-anhyrdo group necessary to form a helix (Figure 1). (F. van de Velde, 2012)

Fig. 1 Chemical structure of lambda, iota and kappa-carrageenan (F. van de Velde, 2012)

Κ-carrageenan gels are hard, strong and brittle gels, ι-carrageenan gels are soft and weak gels and λ-carrageenan does not form a gel but is frequently used as a thickener. The gelation of kappa and iota carrageenan is due to helix formation, which occurs by cooling a heated solution of carrageenan. At temperatures of 60 °C or higher, the polymer chains are in a random coil conformation. After cooling down and passing the coil-helix transition temperature, the carrageenan forms helices. The gels are thermoreversible, meaning that the gels melt when heated but form a gel when cooled. (Hermansson, 1991)

The mechanism involving the gel formation of kappa-carrageenan and the influence of salt are not well understood. Tako et al. (1985) describes the interaction of cations as intramolecular cation-selective bridge. The sulfate esters (SO3-) and 3,6-anhydro group of κ-carrageenan interacted with the positively charged cations. The cation selective bridge is formed in the presences of large-site cations i.e. K+ , RB+ , Cs+, but does not form in the presence of small cations Na+ and Li+. Morris et al. (1980) found that domains were formed of “side-by-side’ helix-helix aggregations. Carrageenan gel and especially kappa-carrageenan needs specific cations to form these aggregates. The helix-helix aggregation is also called helices clusters, fibers, double helices, super strands or super helical rods. In the model of Morris cations form intermolecular bridges (Figure 2).

Fig.  2 Left: Intramolecular cation-selective bridge (Tako M., 1986), Right: Intermolecular helix-helix aggregation ●: K+ ion (Morris Edwin R., 1980).

## Transmission electron microscopy

The main advantage of transmission electron microscopy (TEM) compared to light microscopy is its high spatial resolution. Resolution in microscopy indicates the smallest distance between two points that can be resolved. Humans can see a resolution between 0.1 and 0.2 mm with their eyes. Higher resolutions can be obtained with microscopes. Light microscopy, for example has a resolution of approximately 200 nm. For light microscopes a higher resolution is not possible, because the smallest wavelength of visible light is 400 nm (violet). For a higher resolution a smaller wavelength is necessary. Electrons can behave like a particle but also like a wave. The wavelength of the electron depends on the accelerating voltage. By increasing the accelerating voltage, the wavelength of the electrons decreases. An accelerating voltage of 100 KeV results in a resolution of 4 pm (0.004 nm). So in theory it is possible to see atoms with an electron microscope, because the resolution is lower than the diameter of an atom. However in practice this is not possible because of limitations of lenses. A spatial resolution of 0.1 nm is possible nowadays. (D. B. Williams, 1996)

### Setup

A TEM works schematically like an old slide projector. A slide projector has five main elements; a light source, condensing lens, a slide holder, focusing lens and a screen. A TEM has in principle the same five main elements. An electron gun is used to emit and accelerate electrons towards the sample, just like a light source. The electrons are focused using magnetic coils and lenses. Condenser and objective aperture are holes along the column of the microscope that define the size of the electron beam to change the contrast and resolution. Instead of light passing through the slide holder and projecting on the screen, electrons passing through the sample and are detected by a cathode ray tube detector or a sensitive camera that creates the images. The chambers of the microscope are under high vacuum, to avid that the electrons interact with air molecules before passing through the sample. In figure 3 a TEM setup (left) and a schematic overview of the TEM (right) are shown. (Niederstrasser, 2015)

Fig.  3 Picture of transmission electron microscope (left), schematic overview of setup of the TEM (right). (Niederstrasser, 2015)

### Sample

There are a few requirements for the sample preparation to get high quality images. The specimens should be thin (100 nm or less), otherwise all the electrons are absorbed or reflected. With a high accelerated voltage a thicker sample can be used, but thin samples are easier to handle. Cutting thin sections is done with an ultra-microtome. The thin sections are placed on a grid (Figure 4). Because of the high voltage between 100 and 200 KeV the electrons have a higher energy and can damage the sample. The specimen is bleached or damaged. Three-dimensional (3D) reconstructions can be made with a series of images acquired at different angles (tomography).

The sample preparation method or the thinning process is very time consuming (at least four days) and has an effect on the structure of the sample. Another limitation of imaging with the TEM is that one can only image a small part the sample. Due to the difficulties with sample preparation and handling, there is a need for alternative methods such as nanoprobe diffusometry. (D. B. Williams, 1996) (Niederstrasser, 2015)

Fig.  4 Overhead view of a grid diameter 3.05 mm, showing the mesh (top), side view of a carbon coated grid with sample (bottom) (Niederstrasser, 2015).

## Nanoprobe diffusometry

In foods, the characterization of structure at different length scales is very important for understanding of the macroscopic properties, such as taste, mouthfeel, controlled release and delivery, water retention capacity and barrier properties. Biopolymers such as polysaccharides and proteins are forming the multiscale network structures in food. Understanding of how the biopolymer strands are clustered, linked and organized will improve our understanding of the network formation on various length scales ranging from nano- to millimeters. Although direct visualization is possible with transmission electron microscopy (TEM) the sample preparation of this method is very time consuming and is likely to influence the network properties. Nanoparticle diffusometry is a new analytical method in which nanoparticles are used as ‘probes’ that move through the network. Monitoring the position of each probe as a function of time is used to infer properties of the surrounding networks. The Brownian motion of the nanoparticles will probe the network. The size of the nanoparticles determines their self-diffusion behavior in polymer networks, too large nanoparticles will get stuck and too small nanoparticles are not influenced by the network. A nanoparticle that is a little smaller than the pores of the network, is not immobilized but hindered by the strands of the biopolymers and therefore characterizes the network. The nanoprobes should not interact chemically with the network or stick to it. Analytical techniques that can be used to measure the self-diffusion of nanoprobes are optical microscopy, fluorescence microscopy and pulsed-gradient spin echo nuclear magnetic resonance (NMR). This study will focus on fluorescence microscopy and the two associated techniques: fluorescence recovery after photo bleaching (FRAP) and total internal reflection microscopy (TIRFM). (D. de Kort, 2015)

Fig. 5 Dendrimer-G5-Atto

Commonly used nanoparticles are, for example, flexible polymers made of dextran, a branched polysaccharide or polyethylene glycol (PEG). In solution, the polymers form random coils, but in a denser environment the polymers can form particles. This type of formed particle is a dynamic particle, but there are also nanoparticles that are rigid and spherical. A broad range of rigid particles has been studied, for example proteins and solid gold colloidal nanoparticles. Recently introduced nanoparticle are so-called dendrimers, macromolecules consisting of repeating branched units. The diameter of dendrimers is typically between 1 and 10 nm. For probing the biopolymer network, the dendrimer has to be coated with a neutrally charged, water soluble polymer so that it does not stick in or to the network. PEG, poly vinyl alcohol and dextran can be used for this. For the application of the nanoparticles measured with fluorescence microscopy, the particles should be labeled with a fluorescent molecule (fluorophore). The nanoprobe for the FRAP experiment is a dendrimer containing ATTO 488 dyes and coated with PEG (Figure 5). (D. de Kort, 2015)

Quantum dots were used for the TIRF experiments. Quantum dots are half-conducting nanocrystals, featuring a high fluorescence quantum yield and a large Stokes shift. The quantum yield describes the probability of emitting a photon after a photon got absorbed. The Stokes shift commonly describes the difference between the maximum excitation and maximum emission. A high Stokes shift makes it easier to separate between the excitation and detection of the quantum dots. The fluorescence emission characteristics of quantum dots depend on their size, which is in the range of 2-10 nm in diameter. Their size can be precisely controlled during the synthesis and so a broad range of quantum dots with different emission spectra are available. Large quantum dots emit light with a longer wavelength. Quantum dots are very bright and do not bleach under the intense laser illumination required for TIRFM. The core of the quantum dots are typically made from cadmium selenide (CdSe) or cadmium telluride (CdTe). The core is surrounded with ZnS shell. The naked quantum dots are only soluble in organic solvents. The semi conductive core can be coated with hydrophilic materials to make the quantum dots soluble in water. (Ute Resch-Genger, 2008)

## CLSM-FRAP

Fig. 6 Confocal microscopy setup with laser (1), dichroic mirror (2), objective lens (3), sample (4), confocal pinhole (5), detector photomultiplier (6). (M. B. Dürrenberger, 2001)

Confocal Laser Scanning Microscopy (CLSM) uses lasers to excite the fluorophores in a well-defined sample volume and detect their fluorescence. In contrast to a conventional wide field optical epi-fluorescence microscope a CLSM can produce optical sections through a three-dimensional specimen. The reason that a CLSM can obtain information from one focal plane only is the use of a confocal pinhole placed before the detector. The pinhole is a screen with a small hole that allows only the light originating from the focal plane to pass (Figure 6). Images are composed from point detections by raster scanning through the sample. Using CLSM for fluorescence recovery after photo bleaching (FRAP, further explained below) defined bleach spots can be made in a thin section. The resolution of a CLSM is ≥0.25 μm, so an average diffusion of the nanoprobes is measured with FRAP. (Davidson, 2012) (M. B. Dürrenberger, 2001)

FRAP experiments are widely used in to monitor diffusion and movement of molecules in living cells, membranes and other biological systems. In these experiments, lipids or proteins are labeled with a fluorescent dye. For the characterization of biopolymer networks, freely-diffusing fluorescent nanoprobes were placed in the carrageenan gel. FRAP experiments were performed on a confocal laser scanning microscope (CLSM) allowing to achieve a high resolution in a small depth of the sample. The principle of FRAP is to photo bleach in a defined region of the sample with a short intense laser pulse. Therefore a specific (bleach) spot is selected and the intensity of the fluorescence in this spot is monitored as a function of time. Initially, the free diffusing fluorescence nanoprobes (fluorophores) in the spot are bleached due to the high intensity laser pulse, thus reducing fluorescence intensity in the spot. Immediately after the bleaching, unbleached nanoprobes from outside the bleached area diffuse or move into the bleached spot. Resulting in a recovery of the fluorescence. A FRAP curve is obtained by plotting the intensity of fluorescence in the bleach spot in time (Figure 7). The plot can be used to measure the fraction of mobile nanoprobes and their mobility (diffusion coefficient). (Eils, 2004)

5

4

3

1

2

Fig.  7 FRAP curve with the fluorescence intensity plotted in time (s).

Settings FRAP

The dendrimers are small (7 nm) and very fast diffusing. To follow the diffusion, it is necessary that the CLSM acquires as many images (frames) as possible per second. A scan speed of 1400Hz line frequency and bidirectional scan is recommend to use. Bidirectional scanning means that the laser not only goes from left to right but also directly back from right to left. The format from the images is responsible for the pixel size; a small format and large pixel size gives a fast scanning of the image. Because of the fast scanning the field of view must be small, a zoom factor is required. The gain can be used to achieve more contrast and intensity. However a high gain will increase the noise, the highest signal-to-noise ratio can be achieved at a gain of 800. The bleach format is the selected spot of bleaching, the size of the bleach spot influences the diffusion. As a rule of tumb a larger spot is used for rapidly diffusing particles and a smaller one for more slowly diffusing particles (Eils, 2004). Those were some of the factors that needed to be optimized. The intensity of the lasers has to be sufficiently high during bleaching and low during image recording so no bleaching occurs. The fluorophore has an excitation peak of 450-515 nm and emission peak of 523 nm (ATTO-TEC, 2015) and was therefore excited at 488 nm and the fluorescence was detected between 505 and 605 nm. In table 1 an overview of the selected settings is shown.

Table 1. Settings for FRAP experiment

| Setting |  | Setting to optimize |
| --- | --- | --- |
| Objective | 10x6 | Bleaching spot size |
| Exciting λ | 488 nm | Intensity laser imaging |
| Detection λ | 505-605 nm | Intensity lasers bleaching |
| Gain | 800 | (Pre- /post- ) bleach time |
| Format | 512x512 | Pinhole size |
| Speed | 1400 Hz |  |
| Bidirectional | On |  |

### FRAP data analysis

Equation 1 describes the relation between the diffusion coefficient (D), the radius of the bleach spot (w) and the recovery half-time (t1/2). The recovery half-time is the time it takes for the fluorescence to recover to 50% of the asymptotic intensity. The half-time depends on the experimental settings and conditions such as bleaching spot size and temperature. The half-time can be obtained from the FRAP curve by fitting an exponential function (2). F is the fluorescent intensity, a is the amplitude, t is the time, Ԏ is the time constant of recovery and c the offset. However this is an estimation of the diffusion coefficient, because this equation makes the assumptions that the bleach spot is a flat spot and diffusion occurs only in 2D. In reality the fluorophores diffuse random in all directions. (Eils, 2004)

D=0,88*w24* t1/2                                          (1)

F=a*1-exp-tτ+c          (2)

t1/2= τ*ln2                                (3)

## TIRFM and single particle tracking

Total internal reflection fluorescence microscopy (TIRFM) uses total internal reflection between the glass and the sample to illuminate a thin layer (~100 nm) in the sample. The small excitation volume reduces the background thereby increasing the obtainable signal to noise ratio. Allowing to detect single fluorescent molecules. This is why single particles can be then tracked and the diffusion coefficient can be measured with TIRFM. Total internal reflection happens when light travels from a medium with a higher reflection index to a medium with a lower reflection index for example from glass to water. If the angle of incidence is higher than the critical angle, the light is in total internal reflection. This means that the light is reflected and at the same time an “evanescent field” is produced. The evanescent field is a thin electromagnetic field with the same frequency as the incident light. The field exponentially decease in intensity with increasing distance from the surface, so that only the fluorophores near to the surface are excited. Snell’s law describes the relationship between the angle of incidence (θ1) and the angle of the refraction/reflection (θ2) when light traveling the interfaces of two transparent materials with different refractive indexes (n1 and n2). Snell’s law can also determine the critical angel (θc), this is the largest possible angle of incidence which still results in a refracted ray. The critical angle can be determined by filling in the refractive index and a refraction angle of 90 degrees (see equation 4 and Figure 8). (Axelrod, 2001)

Snell's law: Sin θ1Sin θ2=n2n1             (4)

Fig.  8 Light traveling from a medium with a high refraction index to a medium with a low refraction index (n2), because θ1 is bigger than θc the light is in total internal reflection (right) and an evanescent field is produced. (Josell, 2016)

### Single particle tracking and data

Instead of images made of quickly scanning the sample in CLSM, TIRFM uses a camera to acquire movies from individual wide-field images. In these images fluorescent spots are detected, localized and position-time tracks are calculated using Matlab software. There are two ways to obtain the diffusion coefficient from these tracks. The first method is the mean square displacement (MSD) of the particles in time and the second method is the cumulative probability distribution (CPD) function. The MSD increases linearly in time for normal diffusion and the slope is proportional for the diffusion coefficient. The diffusion of the nanoprobes in the gel are hindered by the biopolymer network so the MSD will increases in time, but the rate of increase reduces. Determining the MSD from the observed trajectories is used in many studies to analyze the tracking data of single-particles. This method has however the disadvantage that it cannot discriminate between single particles with different diffusion coefficients. This means that if there is heterogeneity in the sample which influence the diffusion of the nanoprobes this will not be measured with the MSD. The second method is to calculate the cumulative probability distribution (CPD) function of finding the particle within a circle with radius r after a given time τ. For a homogeneous population of diffusing particles, a single exponential function can be used to fit the data. A second exponential can be added for a heterogeneous population. The probability (P) that a particle starting at the origin will be found within a distance r from the origin after time τ can be given by the equation 5. Where D is the diffusion coefficient (μm2/s) and σ the localization inaccuracy (μm). (Wildenberg M. J. L., 2010)

Pr2,τ=1-exp-r24Dτ+4σ2                (5)

### Settings

Fig.  9 Epifluorescence (left), Variable angle epifluorescence (middle) and Total internal reflection fluorescence (right). (Catherine A. Konopka, 2008)

Stroboscopic illumination is used, this means that the laser light illuminated for only a small time of the entire acquisition time. When continuous illumination is used for fast diffusing molecules like the quantum dots, the shape will be disturbed and a decrease in localization precision will occur. The TIRF angle has to be adjust to find the best signal to noise ratio. The most challenging step is to find the right settings in Matlab to retrieve position-time tracks and measure the diffusion coefficient. The software uses a tracking window to connect the quantum dot in the first image with the quantum dot which has changed its position due to diffusion in the following image. In fact the kind of microscopy relays on the angle of incidence of the light, although the TIRFM is used also variable angel epifluorescence will be used to go in enough focus for nanoprobe diffusometry in κ-carrageenan gel (Figure 9). (Catherine A. Konopka, 2008)

# Method and materials

## Preparation of k-carrageenan gels

Five carrageenan gels with 2% κ-carrageenan, 20 mM KCl (for analysis, Merck) and various sodium chloride concentrations (0, 50, 100, 150 and 200 mM, for analysis, 99,5% Merck) were made. The salt solutions were made by weighing the salt with an analytical balance ( Kern & Sohn, Germany) and dissolving the salt in Milli-Q water. The gels were made by weighing 0.5 g κ-carrageenan powder (sulfated plant polysaccharide, Sigma Life Science) in a tube and adding 25 mL salt solution. The κ-carrageenan powder was then dissolved by heating the solution in a water bath (GFL, Germany) at 90 °C for 20 minutes. The biopolymer network was formed during cooling of the gels to room temperature. The gels were thermo reversible.

## TEM characterization of κ-carrageenan gels

The sample preparation of the κ-carrageenan gels consisted of five steps: staining, fixation, dehydration, embedding and cutting.  Appendix A. describes the method for staining, fixation, dehydration and embedding. Appendix B. the method of trimming and cutting with ultramicrotomy using the microtome (Leica ultracut UC7, M26). Thin sections of 70 and 150 nm were made and placed on copper-grids (FCF200-CU Formvar/Carbon 200 Mesh, Copper Electron Microscopy Science). Figure 10 shows all the steps of the sample preparation method for TEM imaging.

The samples were imaged using a Transmission electron microscope (FEI, Tecnai 20) with a single tilt holder kept at room temperature. An accelerating voltage of 200keV and a spot size 2 was used. Images are taken with a MegaView G2-14 bits (TVIPS) camera, exposure time 200 ms, resolution mode 1376x1096 pixels and 8 bit. For a better contrast, a droplet of 10 nm gold particles (410,11 Golsol AURION) was added to the thin sections on the grid. Each of the five gels was imaged at a magnification of 15000x and 62000x. A background correction and 5% percentile stretching was applied on the images with Fiji ImageJ software. Figure 11 shows a flow diagram of the method of imaging.

Fig. 10 Sample preparation consisting of fixation, dehydration, embedding and cutting (Zou, 2016)

To make a three-dimensional (3D) reconstruction of the κ-carrageenan networks, a series of images were taken at a magnification of 19000x. This was done for the 0 mM NaCl κ-carrageenan gel and the 200 mM NaCl κ-carrageenan gel. The holder with the sample was turned to -55° and images were taken every 5° until +60° in an automated manner.

Fig. 11 Flow diagram of the methods used for imaging the biopolymer networks of carrageenan gel with transmission electron microscopy

## CLSM-FRAP

Imaging was done using a Leica TCS-SP5 confocal microscope with the DMI6000 inverted microscope. This system is equipped with 3 lasers: an Argon laser (75 %) multi-line which produces 5 emission lines at 458 nm, 476 nm, 488 nm, 496 nm and 514 nm, a Diode-Pumped-Solid-State (DPSS) emitting at 561nm and a Helium-Neon (HeNe) laser emitting at 633 nm. Acousto-optic tunable filter (AOTF)-controlled laser lines allow a free selection of the excitation lines and individual line alteration. The laser light was focused on the sample by a 10x microscope objective (NA= 0.4, HCX PL APO CS 10.0x0.40 DRY UV). For fluorescence detection, a PMT (photomultiplier tube) detector was used.

Some FRAP settings had to be optimized. Fixed and optimized setting are shown in table 2. These settings were used for all the five κ-carrageenan gels. Six FRAP curves per gel were measured. The nanoprobes PEGylated ATTO-G5-488-labelefgd dendrimers (8.3 mM, diameter 6.0 ± 0.8 nm as determined by FCS) was diluted 20 times in Milli-Q and the FRAP curve was measured five times. Background fluorescence signal was measured on 0 mM NaCl κ-carrageenan gel and 200 mM NaCl κ-carrageenan gel without any dendrimers. For background quantification, three images were taken and the mean fluorescence intensity with 95 % confidence interval was measured.

Table 2 Fixed setting and optimized setting for FRAP experiment

| Setting |  | Optimized settings |  |
| --- | --- | --- | --- |
| Objective | 10x6 | Bleach spot | 50 μm |
| Exciting λ | 488 nm | Intensity laser imaging | 2% |
| Detection λ | 505-605 nm | Intensity lasers bleaching | 100 % |
| Gain | 800 | (Pre- /post- ) bleach time | 50-10-500 |
| Format | 512x512 | Pinhole size | 1 airy 53,66 μm Thickness 6,23 μm |
| Speed | 1400 Hz |  |  |
| Bidirectional | On |  |  |

Fresh carrageenan gels were made, but before cooling down 20 μl of the nanoprobes G5-ATTO dendrimers were added to 2 ml of each of the five κ-carrageenan gels and mixt. After cooling down, a 5x5x5 mm cube was placed on a micro cover slip (24x50mm, 170 ± 5 μm, Brand)

## FRAP data analysis

The obtained FRAP curves (representing the fluorescence intensity inside the bleached spot plotted over time) were corrected for the background fluorescence and the side effect of bleaching during imaging.

The background correction (Ftc1) was performed by subtracting the mean fluorescent intensity from the background gels (Fbackground) from the fluorescent intensity’s during imaging (Ft), as shown in equation 6.

Ftc1=Ft- Fbackground				(6)

The data was also corrected for photobleaching during imaging (Ftc2), shown in equation 7. The fluorescence intensity of the reference spot at time is 0 seconds (Fpre ROI 2) was divided by the fluorescence intensity of the reference spot at time is t (Fpre ROI 2) and multiplied with the corrected fluorescence intensity inside the bleach ROI at time t (Ftc1).

Ftc2=Ftc1* Fpre ROI2Ft ROI 2

(7)

Normalization was preformed following equation 8. The corrected fluorescence intensity inside the bleach ROI immediately after bleaching (F0) was subtracted from the corrected fluorescence intensity inside the bleach ROI at time t (Ftc2) and the corrected fluorescence intensity inside the bleach ROI at time is 0 seconds (Fpre) and divided.

N= Ftc2-FoFpre-F0

(8)

The corrected and normalized curves were used to calculate the diffusion coefficient. Therefore, curve fitting was performed using TableCurve 2D v4 and equation 9. There were two unknown parameters; the amplitude (a) and tau (Ԏ)
N=a*(1-EXP-tԎ) 					(9)

Ԏ was used to calculate the recovery half-time (t½ ) in seconds using equation 10.

t½ = Ԏ * ln 2						(10)

D= 0,88* w24*t½

The diffusion coefficient was calculeded with equation 11. The radius of the bleach spot (w) was 25 *10-6 m.

(11)

In the application letter from Leica an immobile fraction in measure following equation 12. 
Immobile fraction=(Fpre-Feind)(Fpre- F0)*100 %		(12)

Instead of using equation 12 the immobile fraction was determined as one subtracted with the average normalized fluorescence at t= 78 s (equation 13). This is a similar way of calculating the immobile fraction, because Fpre is normalized so one and F0 is normalized to 0. Feind is the corrected and normalized fluorescent signal at the time the equilibrium has been reached. At this time there is none or almost none recovery of the fluorescent signal.

Immobile fraction=1- Fn t=78s*100%		(13)

## CLSM images trapped fraction

To visualize the immobile fraction of G5-ATTO dendrimers in the κ-carrageenan gels, the gels were washed to get rid of the mobile fraction. A cube of approximately 5x5x5 mm was cut from each gel and placed in a 10 ml flask. 5 ml salt solution, with a salt concentration equal to the one used during sample preparation, was added to each flask and removed after 2 hours. Again, 5 ml salt solution was added and removed after two hours. For the final washing step, 5 ml salt solution was added and kept overnight before removing it. The gels in salt solution were kept in the refrigerator. This was done for two sets of fresh made carrageenan gels samples with 20 mM KCl.

The washed gels were placed on a micro cover slip (24x50mm, 170 ± 5 μm, Brand). A background images was taken of a 200 mM k-carrageenan gel without dendrimers. The settings are shown in table 3.The images were analyzed with Fiji ImageJ software to measure the mean intensity and standard deviation of the images. For this purpose a circular area in the middle of the image was used.

To make sure the mobile fraction was washed out, a FRAP experiment was performed on the washed gels. The same settings as for the unwashed gels was used. The washed gels were measured in duplo.

Table 3. CLSM settings of imaging the washed gels

| Setting |  |
| --- | --- |
| Objective | 10x1 |
| Exciting λ | 488 nm 2% |
| Detection λ | 505-700 nm |
| Gain | 1250 |
| Format | 1024x1024 |
| Speed | 10 Hz |
| Pixel size | 1,5 μm |

## TIRFM single particle tracking of QD’s in κ-carrageenan gels

Quantum dots (QD_50 L/E with lipoamide-TEG-11-oME_JB ten Hove) were used for the single particle tracking with TIRF microscopy. These quantum dots (QD’s) were custom made at the BioNanoTechnology department at the Wageningen University. The diameter was approximately 3.7 nm and the stock concentration 17 μM determined by fluorescence correlation spectroscopy (FCS). The emission and absorption spectra of the quantum dots were measured. An absorption spectrum from 200 till 800 nm was taken with an UV-VIS spectrometer (Cary 4000, Agilent Technologies) the quantum dots were 100 times diluted. The emission spectrum was measured with a Fluorolog (Josin yvon-spex). The quantum dots were diluted 2000 times and emission was done with 400 nm laser.

A home-built TIRF microscope set-up in the Laboratory of Biophysics, Wageningen was used. This set-up uses a Lighthub® Omicron laser engine that can independently emit laser light with four different wavelengths (405 nm, 473 nm, 561 nm and 640 nm). An ASI XY stage is built on top of a microscope objective (100x NA 1.49 Nikon). The angle of incidence of the laser light was adjusted manually. The fluorescent signal could pass several bandpass filters after which the signal was split using a set of dichroic mirrors into three different detection channels: blue channel (480-550 nm), a green channel (570-620 nm) and a red channel (660-780 nm). The fluorescence signal was detected by an Andor IXON-897 Ultra emCCD camera (Andor). The camera records signals with a pixel size of approximately 124 nm/pixel. In figure 12 the setup is shown. (Vink, 2015)

Fig. 12 Home-built TIRFM setup laboratory of biophysical Wageningen University.

The cover slips (Menzel-Gläser, 24x60 mm, #1.5) were burned at 500 °C in a oven (Vecstra Furnaces) to get rid of all contaminations. 25 μL of a 30000 diluted quantum dots solution was pipetted on the cover slip. The quantum dots were excited with the green laser (561 nm) and stroboscopic illumination. The settings are shown in table 4.

Table 4 Overview of setting for the TIRF microscope doing single particle tracking.

| Setting |  |  |  |
| --- | --- | --- | --- |
| Acquisition time | 10 ms | Frames | 1000 |
| Illumination time | 1 ms | Localization threshold | 2-1 |
| Exciting λ | 405 nm | Tracking window | 20 |
| Intensity | 60-90% | Pixel size | 124 nm |
| Detection λ | Green and red channel | Format | 170x255 pixels (max 512x512) |

To measure the quantum dots diffusing in the κ-carrageenan gels, the gels were molten and 225 μL of each gel was pipetted in a well of a μ-Slide 8 well (IbiTreat, Germany). 25 μL of a 5000x diluted quantum dot solution was added on top of the gel after cooling down making the quantum dots concentration 0.34 nM. After two hours, the slide was placed on the objective of the microscope and the quantum dots had diffused in the network. A video of 1000 images each representing 10 ms acquisition time was taken five times for each gel.

The quantum dots were washed out of the gel and the trapped quantum dots were imaged. 990 μL of molten κ-carrageenan gel with 0 mM and a 200 mM NaCl was added to 10 μL of a 100x diluted quantum dots solution. After cooling down and waiting for two hours the gels where washed. A 5x5x5 mm cube of the gel was placed in a flask. 5 ml of the salt solution equal to the one used during sample preparation was added. The washing consisted of three steps. For the first two steps fresh salt solution was added and removed after two hours. In the last washing step, the gels were kept in salt solution overnight. The washed gels were imaged with TIRFM.

# Results and discussion

## TEM characterization of κ-carrageenan gels

The biopolymer network of carrageenan was visualized with 2D and 3D reconstruction images made with transmission electron microscopy (TEM). A background correction and 5% percentile stretching was applied on the images with Fiji ImageJ software. In appendix C, figure 32 and 33 an image is shown before and after these corrections. In figure 13, the 2D TEM images of the κ-carrageenan gels with different sodium chloride concentration are shown. The images are made at magnification 150000 x and represent an area of 375x375 nm. The black circler spots in figure 13A and 13B are 10 nm gold particles used for focusing and contrast. The 2D TEM images give a first impression of the biopolymer network in κ-carrageenan gels with different sodium chloride concentrations. In the 0 mM NaCl gel, two different networks were observed. The first network (Figure 13A) is a dense network with small mesh size, the second network is coarser (Figure 13B). The 0 mM NaCl gel has a heterogeneous network, because it consists of a dense and coarse network. In the 50, 100, 150 and 200 mM NaCl κ-carrageenan gels, only a coarse network was found (Figure 13C, 13D, 13E and 13F) and are therefore homogenous networks. To get a representative view of the biopolymer networks in the κ-carrageenan gels, many more images would have to be taken. This was not done due to time constrains. In appendix C, the images of the biopolymer networks in κ-carrageenan gels at a magnification of 62000 x are shown. For the 0 mM NaCl κ-carrageenan gel, again a denser network is seen than for the high sodium chloride concentration κ-carrageenan gels.

With a series of images, a 3D reconstruction of the biopolymer networks in the κ-carrageenan gels could be made for the 0 mM NaCl κ-carrageenan gel and for the 200 mM NaCl κ-carrageenan gel. The 3D reconstructions are shown in figure 14 and 15. The contrast of the 0 mM NaCl κ-carrageenan gel was too low to perform full background subtraction. For this reason there is still considerable noise in the image. The contrast of the 200 mM NaCl κ-carrageenan gel was sufficient for the whole reconstruction as shown in figure 20. This issues with the first image made it difficult to compare both networks, but it seems that the networks are of the similar density. With the 2D TEM, a dense network for the 0 mM NaCl κ-carrageenan gel and a coarse network for the 200 mM NaCl κ-carrageenan gel was found. The 3D reconstruction showed a coarse network for both 0 mM and 200 mM NaCl κ-carrageenan gels. Most likely the dense network was more fine and therefore had less contrast.

To find the correct focus of the 0 mM 2D images, gold particles were added on top of the sample. The gold particles are somehow distracting from the network. To avoid using the gold particles, an extra staining step could be added for example with leadcitrate or uranylacetate. This stainings are very toxic and harmful thought and therefore ideally avoided.

Fig. 13 2D TEM biopolymer networks in κ-carrageenan gel, representing 375x375 nm, A: 0 mM NaCl dense network, B: 0 mM NaCl coarse network, C: 50 mM NaCl coarse network, D:100 mM NaCl coarse network, E: 150 mM NaCl coarse network and F: 200 mM NaCl coarse network.

Fig. 14 3D reconstruction  representing 3.8 μm x 3.8 μm x 0.35 μm, coarse networks in 0mM NaCl κ-carrageenan gel @ Gerard van Dalen

Fig. 15 3D reconstruction  representing 5.0 μm x 5.0 μm x 0.47 μm, coarse network in 200mM NaCl κ-carrageenan gel @ Gerard van Dalen

## CLSM-FRAP assessment of G5-ATTO dendrimer diffusing in κ-carrageenan gels

Fluorescence recovery after photobleaching (FRAP) experiments were performed on κ-carrageenan gels made using different NaCl concentrations of 0, 50, 100, 150 and 200 mM. A FRAP curve of the 0 mM and 200 mM κ-carrageenan gel is shown in figure 16. The fluorescence was measured for 80 seconds for the bleach spot and a reference spot as shown in figure 17. After 18 seconds the bleach spot was bleached for four seconds with high laser power. The time period before bleaching is called pre-bleaching and after bleaching post bleaching, during this period the fluorescence intensity was measured by making images with 2 % laser intensity. The fluorescence intensity of the reference spots degreases in time, for the reference spot of 0 mM NaCl κ-carrageenan gel the fluorescence intensity was 10528 counts at t = 0 s and 9990 counts at t = 80 s. This is the effect of photobleaching during imaging and data acquisition. During post-bleaching the fluorescence intensity in the bleach spot recovers, because of redistribution of bleached and unbleached nanoprobes from outside the bleach area. The fluorescence intensity cannot fully recover back to the level before bleaching due to the unavoidable bleaching during imaging. Therefore the curves have to be corrected for bleaching during imaging. The difference between the 0 mM NaCl and 200 mM NaCl κ-carrageenan gels are the recoveries as will be discussed later. The FRAP curves of all the five κ-carrageenan gels were measured at least five times, all the data are shown in appendix D. The diffusion of nanoprobes in water was also measured with a FRAP curve. In water, the nanoprobes could diffuse free through Brownian motion as for the nanoprobes in the gel can be expected that the self-diffusion of nanoprobes is hindered by the biopolymer network. The FRAP curves of the nanoprobes in water are shown figure 43 appendix D.

Fig. 16 FRAP curves — : 0 mM NaCl κ-carrageenan gel bleach spot …: 0 mM reference spot — : 200 mM NaCl κ-carrageenan gel …: 200 mM reference spot

Fig.  17 snapshot FRAP, on 100 mM κ-carrageenan gel with bleach spot (middle) and reference spot (upper right) representing 258x258 μm

The data had to be corrected for the background fluorescence. The background fluorescence was measured for a 0 mM NaCl κ-carrageenan gel and 200 mM NaCl κ-carrageenan gel prepared without fluorescent dendrimers. Six images were made for each gel. The average fluorescent intensity with 95% confidence interval was 1080 ± 40 counts for the 0 mM NaCl gel and 1100 ± 30 counts for the 200 mM NaCl gel. These intervals overlap, so there is no significant difference between the background levels. The data could be merged. The background with 95% confidence interval was 1090 ± 20 counts. For statistics see Appendix E.

The FRAP curves were corrected for the background fluorescence, bleaching during imaging and normalized with equation 6,7 and 8 shown in the Chapter 3. The average of the corrected and normalized curves of 0 mM NaCl and 200 mM NaCl κ-carrageenan gel are shown in figure 18. The average FRAP curves of the other gels are shown in appendix F. In figure 19 the average FRAP curve of self-diffusion of nanoprobes in water is shown.

Fig. 18 Average corrected and normalized FRAP curves with 95% confidence interval — : 0 mM NaCl κ-carrageenan gel — : 200 mM NaCl κ-carrageenan gel

Fig. 19 Average corrected and normalized FRAP curves with 95% confidence interval of dendrimers diffusing in water.

A diffusion coefficient could be calculated from the FRAP curves by fitting equation 9 and calculated the recovery half time (equation 10) and the diffusion coefficient (equation 11).

The first 25 points after bleaching (9 seconds) of nanoprobes in water were fitted with equation 9, show in figure 20. In the fitted equation 14 0.515 is the amplitude and 2.76 is tau. Tau was multiplied with ln 2 to get the recovery half time. With the recovery half time the diffusion coefficient could be measured. The diffusion coefficient was measured with equation 11. The radius of the bleach spot (w) was 25 *10-6 m. This was done for all the five measurement. In table 5 the fitted parameters and measured half time and diffusion coefficient are shown.

D=0.88 w2 4 t12= 0.88 (25 *10-23)2 4*2.76= 7.19 *10-11 m2/s 				(11)

F=0.515*(1-EXP-t2.76) 							(14)

Fig. 20 Corrected and normalized fluorescence over time the first 25 points after bleaching for free dendrimer (1) with F: 0.515 *(1-EXP-t2.76) r2:0.978.

Table 5. Parameters equation 7 with r2 and the measured recovery half time (t½) and the diffusion coefficient for 5 measurements of dendrimer in water.

| parameters | (1) | (2) | (3) | (3) | (5) |
| --- | --- | --- | --- | --- | --- |
| a | 0.52 | 0.49 | 0.49 | 0.48 | 0.65 |
| Ԏ | 2.76 | 2.45 | 2.67 | 2.57 | 3.19 |
| r2 | 0.978 | 0.982 | 0.979 | 0.985 | 0.994 |
| t½ (s) | 2.76 | 2.45 | 2.67 | 2.57 | 3.19 |
| D (m2/s) | 7.19E-11 | 8.11E-11 | 7.43E-11 | 7.71E-11 | 6.22E-11 |
| D (μm2/s) | 71.9 | 81.1 | 74.3 | 77.1 | 62.2 |

The average diffusion coefficient for the free dendrimer was measured with 95% confidence interval and was 73 ± 9 μm2/s.

The Stokes-Einstein equation (equation 15) is the relationship between the diffusion coefficients (D) of a spherical particles with radius (RH). The equation was used to predict the diffusion coefficient of the free diffusing dendrimer in water in m2/s.

The Boltzmann constant (KB) is 1.38*10-23 J/K, the absolute temperature (T) is 294.14 K for 21 °C, the viscosity of water (η) is 1 mPa*s and the hydrodynamic radius of the G5-ATTO dendrimer (RH) 3.0 ±0.4 nm.

Dmax= KBT6 π η RH= 1.38 *10-23*294.146 π* 0,001*(2.6*10-9)=8.29 *10-11 m2/s 			(15)

Dmin= KBT6 π η RH= 1.38 *10-23*294.146 π* 0,001*(3.4*10-9)=6.34 *10-11 m2/s 			(15)

The theoretical diffusion coefficient is the average of the minimum and maximum diffusion coefficient measured with the Stokes-Einstein equation. The theoretical diffusion coefficient of dendrimer in water (21°C) is 73 ± 10 μm2/s and is in excellent agreement with the measured diffusion coefficient (73 ± 9 μm2/s).

The FRAP curves of the κ-carrageenan gels were also fitted to measure the diffusion coefficient, see table 6. The diffusion coefficients of the nanoprobes in the gel was between 103 and 150 μm2/s. Expected was that the self-diffusion of nanoprobes would be hindered by the biopolymer network and the diffusion coefficient should decrease. The diffusion coefficient of the dendrimer in water was 73 ± 9 μm2/s. The diffusion coefficients of the nanoprobes in the gels are faster than the nanoprobes in water. The nanoprobes in water can diffuse free through Brownian motion, it would be most unlikely that they would diffuse faster in the gels. The FRAP curves were corrected for bleaching during imaging, but this dependents on the reference spot. Also the equation used for measuring the diffusion coefficient used the estimation that there is only two-dimensional diffusion, however the nanoprobes diffuse through Brownian motion so three-dimensional. (Eils, 2004)

| [NaCl] mM | Diffusion coëfficiënt μm2/s |
| --- | --- |
| 0 | 129 ± 15 |
| 50 | 119 ± 12 |
| 100 | 150 ± 16 |
| 150 | 106 ± 30 |
| 200 | 103 ± 16 |

Table 6. Measured diffusion coefficient with standard deviation of the nanoprobes in κ-carrageenan gel with different sodium chloride concentrations

The immobile fraction of nanoprobes in the κ-carrageenan gels calculated following equation 13. The average normalized and corrected fluorescence at 78 seconds was used for this calculation. In table 7 the calculated immobile fraction with 95% confidential interval is shown for each gel with different sodium chloride concentration. These values where plotted in figure 21. An immobile fraction was also calculated for the nanoprobes in water as shown in table 7.

Immobile fraction=(1- Fn t 78s) * 100 %		(13)

Table 7. Immobile fraction with 95% confidential interval.

| [NaCl] | 0 mM | 50 mM | 100 mM | 150 mM | 200 mM | water |
| --- | --- | --- | --- | --- | --- | --- |
| Immobile fraction % | 62 ± 4 | 49 ± 6 | 49 ± 3 | 25 ± 5 | 23 ± 8 | 12 ± 8 |

Fig.  21 Calculated immobile fraction in κ-carrageenan gel with different sodium chloride concentrations with 95% confidential interval

There is a relation between the concentration of sodium chloride and immobile fraction in the κ-carrageenan gels. The lower the NaCl concentration the higher the immobile fraction. An immobile fraction indicates that a part of the nanoprobes is trapped or damaged. A small part of the nanoprobes is bleached and damaged. For the bleaching during imaging, a correction was performed. It was expected that the nanoprobes diffusing in water had a negligible immobile fraction, but the immobile fraction was still 12 ± 8 %. It could be possible that a small part of the nanoprobes was non-specifically absorbed on the glass surface. However the immobile fraction of the nanoprobes in water is the smallest of all the calculated immobile fractions. With TEM it was concluded that the network of the κ-carrageenan gel without NaCl was dense. The immobile fraction indicates the amount of the nanoprobes that is trapped in the biopolymer network and can be used to characterize the network.

## CLSM characterizing trapped G5-ATTO dendrimer in washed κ-carrageenan gels

Two sets of washed κ-carrageenan gels with different sodium chloride concentration were imaged with CLSM to visualize and measure the immobile/ trapped fraction of nanoprobes. In figure 22 one set of washed carrageenan gel with different sodium chloride concentrations and the background is shown. The background was taken from a 200 mM NaCl κ-carrageenan gel without nanoprobes. A second set of images is shown in appendix G. The images represent an area of 1.55 mm by 1.55 mm.

The washed gel without any sodium chloride (0 mM) is very heterogeneous and shows intense fluorescent spots. These spots with a size of approximately 50x50 μm are less frequently present in the washed κ-carrageenan gel with 50 mM NaCl. In the 100 mM, 150 mM and 200 mM NaCl κ-carrageenan gels, no intense spots are visible, but the fluorescent background signal is still higher than the background in the control measurement. The black spots are air bubbles trapped between the sample and the gel.

Fig. 22 Confocal image representing 1,55 x 1,55 mm of washed κ-carrageenan gels of different sodium chloride concentration with trapped nanoprobes serie 1.

A FRAP experiment was applied on the washed κ-carrageenan gels to show that the washed gels consist of only trapped dendrimers. As shown in figure 23, there is no recovery of the fluorescent signal after the bleaching pulse. After washing, the mobile fraction seems to be completely removed and only the immobile fraction is remaining. In the graph, a small increase of fluorescence is visible immediately after bleaching. This is likely to be from the saturation of the detector after full laser power bleaching.

Fig. 23 FRAP curve of 100 mM NaCl washed κ-carrageenan gel the normalized fluorescent intensity plotted over time in seconds

The mean gray value including the standard deviation of the fluorescent signal was measured with Fiji ImageJ software (table 8). The measured background intensity is significantly lower than in all the other gels. This implies there are still nanoprobes trapped in the network after washing. The gray values were corrected for the background and normalized according to equation 16 (table 8). In figure 24, the average relative gray values plotted for the sodium chloride concentration of the κ-carrageenan gels are shown. The gray values of a second set is shown in appendix G.

Relative gray value= mean gray value-maen gray value backgroundmean gray value 0 mM                       (16)

Table 8. Mean, relative and average gray values with standard diviation of the washed κ-carrageenan gels (set 1) with different sodium chloride concentration.

| NaCl Concentration (mM) | Mean gray value (*10-3) | Relative Gray value | Average relative Gray value |
| --- | --- | --- | --- |
| 0 | 36 ± 4 | 1.00 ± 0.08 | 1.00 ± 0.13 |
| 50 | 25 ± 3 | 0.69 ± 0.06 | 0.78 ± 0.10 |
| 100 | 25 ± 3 | 0.68 ± 0.06 | 0.62 ± 0.07 |
| 150 | 21 ± 3 | 0.59 ± 0.06 | 0.56 ± 0.07 |
| 200 | 19 ± 3 | 0.53 ± 0.05 | 0.50 ± 0.06 |
| Background | 0.9 ± 0.3 | - | - |

Fig. 24 Normalized fluorescent intensity of washed gels plotted over the sodium chloride concentration of the gels.

Figure 24 illustrates that the higher the sodium chloride concentration in the washed κ-carrageenan gels the lower the gray value. The gray value is the fluorescent intensity of the images and deepens on the nanoprobes present in the gel. The higher the sodium chloride concentration the less nanoprobes are present after washing the gel. The immobile fraction measured of the FRAP curves was also lower for high sodium chloride concentration κ-carrageenan gels. The network of high sodium chloride carrageenan gel was coarser, because less nanoprobes were trapped. The standard deviation of the gray value of the 0 mM NaCl κ-carrageenan gel is the biggest of all and the 200 mM NaCl the smallest. 0.13 relative for no sodium chloride and 0.06 for 200 mM NaCl sodium chloride. In the image of 0 mM NaCl gel intense fluorescent spots were visible, so there is more variation in the sample. The intense fluorescent spots could be explained as a bulk of nanoprobes trapped in a dense network. The standard deviation of the mean gray value is an indication for the heterogeneity of the biopolymer networks. From the data we can conclude that low sodium chloride κ-carrageenan gels have a heterogeneous network with dense domains in which a lot of nanoprobes can be trapped. Moreover, high sodium chloride κ-carrageenan gels have a more homogenous coarse network in which a few nanoprobes are trapped. This agrees with the conclusion drawn from the experiments done with TEM.

## TIRFM single particle tracking of QD’s in κ-carrageenan gels

For the single particle tracking (SPT) with TIRFM quantum dots were custom made at Wageningen University. The absorption and emission spectra of the quantum dots were recorded and are shown in figure 25. The quantum dots have a broad adsorption wavelength and a maximum absorption around 200 to 250 nm (UV-light). The quantum dots were exited with light of 400 nm wavelength for recording the emission spectrum. The emission maximum is at 670 nm (red light). The spectra shown the high stoke shift of the quantum dots. The maximum excitation and maximum emission wavelength are well separated.

Fig. 25 Light intensity plotted over the wavelength 						       — : absorption spectrum quantum dots — : emission spectrum quantum dots

A movie was made of quantum dots diffusing in water. The movie consisted of 10000 frames acquired with 1 frame representing a 10 ms acquisition time. The quantum dots were exited with 40 % green laser (561 nm). Even though the maximum absorption of the quantum dots is around 200 to 250 nm, the green laser is sufficient to excite the quantum dots effectively. In fact, a photon representing green light has less energy than UV-light and therefor there is less absorption/excitation of other contaminations in the solution. The quantum dots were localized in the each frames as shown in figure 26. The localized spots were connected to form position time tracks. The position time tracks were made by choosing a tracking window. The diffusion coefficient could was calculated with the cumulative probability distribution (CPD).

Fig.  26 Four frames of TIRF movie with position –time track of a quantum dot diffusing in water, representing 21x27 μm

Tracking window

The tracking window is really important for the calculating the correct diffusion coefficient. The tracking window represents the radius in which two localized spots in two successive frames can be connected to form a position-time track. If the tracking window is too small, a diffusing nanoprobe would not be connected and the finally determined apparent diffusion coefficient would be too slow. If the tracking window is too large, however, a miss assignment of two different nanoprobes could occur such that the calculated apparent diffusion coefficient would be faster than the actual diffusing coefficient. The influence of the size of the tracking window on the diffusion coefficient of nanoprobes diffusing in water is shown in figure 27. The diffusion coefficient was measured for a tracking window of 1.24 μm till 3.41 μm (representing 10 - 27.5 pixels).

Fig. 27 Measured diffusion coefficient plotted over the used tracking window with regression D= 36.9 * tracking window -31.6, R2: 0.9912

Fig. 28 Number of steps plotted over the step length for a tracking window of 1.24 μm (left), 2.48 μm (middle) and 3.41 (right)

The step length of the position-time tracks is used to calculate the CPD to measure the diffusion coefficient. In figure 28 the step length for the position-time tracks calculated for a tracking window of 1.24 μm, 2.48 μm and 3.41 μm are shown. The step length cannot be larger than the tracking window, because steps bigger than the tracking window are not tracked. For a tracking window of 1.24 (Figure 28 left) the maximum amount of steps was for a step length of 1.24 μm. This tracking window is too small, because diffusion has a Gaussian distribution as is shown for a tracking window of 2.48 μm. A tracking window of 3.41 (Figure 28 right) looks Gaussian, but the maximum amount of steps was for a step length between 1.25 and 1.50 μm, which is not in the middle. A large tracking window miss assignment will occur. For fast diffusing quantum dots optimizing the tracking window and concentration is really important, but also challenging.

To find the right tracking window, an expected diffusion coefficient and minimum tracking window was measured. The expected diffusion coefficient was calculated with the Stokes-Einstein equation (equation 17). The radius of the quantum dots was 3.7 nm measured with FCS. The measured diffusion coefficient of the nanoprobes in water is 58 μm2/s.

D= KBT6 π η RH   = 1.38 *10-23*294.146 π* 0,001*(3.7*10-9)=5.8 *10-11 m2s=58 μm2/s	(17)

The minimum size of the tracking window can be calculated with equation 18 which describes the relationship of diffusion over distance. X is the mean distance from the starting point that the nanoprobe has diffused in time (t). t is the time per frame which was 10 ms (0.01 s) and D the diffusion coefficient. The tracking window is given in pixels and one pixel is 0.124 μm. The minimum tracking window can be calculated by dividing the mean distance (x) with the pixel size (0.124 μm). For a diffusion coefficient of 58 μm2 /s a minimum tracking window of 2.3 μm (19 pixels) was required.

x2=4*D*t		 						(18)
x2=4*58*0,01

x=2.3 μm/ 19 pixels

Ten movies of quantum dots diffusing in water were analyzed with a tracking window of 2.48 μm (20 pixels) and the diffusion coefficient was measured. The diffusion coefficient was 56 ± 2 μm2 /s (see table 9).

Κ-carrageenan gels

Fig.  29 0 mM NaCl κ-carrageenan gel without nanoprobes, left green channel, right red channel, representing 21x27 μm

To measure the self-diffusion of nanoprobes in κ-carrageenan gels, first a fresh made κ-carrageenan gel without NaCl and quantum dots was imaged. In the green channel some contaminations were visible as shown in figure 29. The red channel however was empty, this was the channel were the quantum dots would be detectable diffusing.

The quantum dot concentration was kept low (0.3 nM), to prevent miss match of the position-time tracks. The quatum dot diffusion in the carrageenan gel was visualized for all the gels, however this concentration was too low to retrieve good position-time tracks for the nanoprobes in all the gels, only the nanoprobe self-diffusion in the 0 mM NaCl κ-carrageenan gel could be measured. Eight movies of quantum dots diffusing in the gel were analysed with a tracking window of 2.48 μm. The calculated diffusion coefficients are shown in table 9. The diffusion coefficient of the quantum dots diffusing in the 0 mM NaCl gel was determined to be 55 ± 2 μm2 /s. There was no significant difference between the diffusion coefficient in water 56 ± 2 μm2 /s and in the 0 mM NaCl gel. Expected was that the quantum dot diffusion was hindered through the biopolymer network in the 0 mM NaCl gel and diffusion was slower. As shown with TEM and FRAP the biopolymer network of no NaCl and low NaCl concentration carrageenan gel consist of a dense heterogeneous network. However this could be measured with single particle tracking of quantum dots. In some videos, a trapped quantum dot was visible, which stayed on the same spot for more than 1.0 s. This was also seen with the immobile fraction of FRAP and CLSM images of washed gel.

Table 9 Measured diffusion coefficients for quantum dots in water and 0 mM NaCl gel with average diffusion coefficient and 95% confidence interval.

| Measured diffusion coefficients (μm2 /s) water |  | Measured diffusion coefficients (μm2 /s) 0 mM NaCL gel |  |
| --- | --- | --- | --- |
| 52 | 57 | 52 | 56 |
| 54 | 57 | 52 | 56 |
| 54 | 57 | 54 | 56 |
| 54 | 58 | 54 | 58 |
| 56 | 58 | - | - |
| Average | 56 | Average | 55 |
| CI 95 % | 2 | CI 95 % | 2 |

Washed gels

Single trapped quantum dots were imaged in washed κ-carrageenan gels with 0 mM NaCl and 200 mM NaCl (Figure 30 and 31). Only the red channel was used to get rid of the contaminations. Both gels showed trapped quantum dots. No difference between the 0 mM and 200 mM NaCl gel was seen. To get a good impression and find the dense network more images had to be made. The diffusion coefficient with tracking window of 20 pixels was measured. The trapped quantum dots had a diffusion coefficient of 0 μm2 /s.

Fig.  30 Washed 200 mM NaCl gel red channel representing 21x27 μm

Fig.  29 Washed 0 mM NaCl gel red channel representing 21x27 μm

## Overall discussion

3D TEM reconstructions showed only the coarse networks in both the 0 mM NaCl and 200 mM NaCl κ-carrageenan gels, whereas 2D TEM showed a dense and coarse network for the 0 mM NaCl κ-carrageenan gel and only a coarse, but not dense, network for all other κ-carrageenan gels (50, 100, 150 and 200 mM NaCl). The staining and thus the contrast was too weak for the dense/ fine networks to be visualized. Gold particles were added to the κ-carrageenan gels with 0 mM and 50 mM NaCl concentration for focus of the dense/fine networks. The gold particles however distract from the biopolymer network and the shadow of the gold particles are spread out in the 3D reconstruction, which hampers reconstruction of the 3D networks.

The TEM images are static snapshots of the network within a small field of view (5x5 μm). For a representative overview of the biopolymer network, many more images would have been required. Furthermore, the sample preparation method for TEM, consisting of five steps (staining, fixation, dehydration, embedding and cutting) is really time consuming. In addition, staining is invasive and not equally effective for different networks. The contrast of dense networks was lower than the contrast of the coarse networks. The advantage of nanoprobe diffusometry for the characterization of the biopolymer network are acquisition speed and a less invasive sample preparation procedure.

The self-diffusion of nanoprobes in κ-carrageenan gels was measured with CLSM-FRAP and TIRFM-SPT. FRAP is a bulk technique in which we analyzed, the immobile fraction and diffusion coefficient in a spot of 50 μm diameter. TIRFM-SPT is a real single particle approach and can therefore provide additional details.

Surprisingly, the calculated diffusion coefficient obtained after fitting the FRAP curves of nanoprobes in the κ-carrageenan gels were faster than freely diffusing nanoprobes in water. Bleaching during imaging is considered to be the main reason for the inaccurate self-diffusion coefficients. Although, the FRAP curves were corrected for bleaching during imaging, the correction might have been compromised by the choice of the reference spot. Furthermore, the equation used for calculating the self-diffusion coefficient departed from the assumption that there is only two-dimensional diffusion, whereas nanoprobes actually diffuse in three-dimensional.

The FRAP experiments indicated that the κ-carrageenan gels with ≤ 100 mM NaCl contained a larger immobile fraction of nanoprobes (above 50%) than the κ-carrageenan gels with high NaCl concentration (150 mM and 200 mM). The presence of an immobile fraction indicates that a part of the nanoprobes is trapped in a dense biopolymer network. The presence of more trapped nanoprobes in the κ-carrageenan gels prepared with 0 mM and 50 mM NaCl (<100 mM NaCl) could also be visualized by performing CLSM on gels where the freely diffusing particles were washed away. The distribution of the trapped fraction of nanoprobes could be imaged and the fluorescent intensity depended on the amount of trapped nanoprobes. A quantitative dependency of the amount of trapped probes could be established. In the 0 mM NaCl and 50 mM NaCl washed κ-carrageenan gels domains (±50x50 μm) of high intensity fluorescence were imaged. Washing of the gel, highlighted the existence of an immobile trapped fraction of nanoprobes and reveals density and heterogeneity at micron scale. The domains correspond to nanoprobes trapped in a dense network. The κ-carrageenan gels with 0 mM and 50 mM NaCl have thus a dense and coarse network and are heterogeneous, whereas the κ-carrageenan gels with 150 mM and 200 mM NaCl comprise a homogeneous and coarse network. The 100 mM NaCl κ-carrageenan gel is an intermediary of this two networks, because the immobile fraction calculated of the FRAP data indicated a dense network, but no domains of high intensity fluorescence were imaged with CLSM.

With 2D TEM, a dense and heterogeneous network was visualized for the 0 mM NaCl κ-carrageenan gel and a coarse network for the other κ-carrageenan gels. CLSM-FRAP provides more information about the heterogeneity and density of the κ-carrageenan gels than the TEM method. The intensity of the gray values of the confocal images of the washed gels and the immobile fraction measured with the FRAP curves was also a quantitative way to characterize the biopolymer networks of κ-carrageenan gels.

TIRFM-SPT using quantum dots diffusing in k-carrageenan gels could be measured, however the right concentration of nanoprobes was not yet established. A quantum dot concentration of 1.7 nM was too high causing miss matches in the position-time tracking, but a concentration of 0.3 nM was found to be to low. For that reason, it was not yet possible to quantify the self-diffusion behavior of the nanoprobes in all the κ-carrageenan gels. More optimization is required in order to quantify the TIRFM-SPT results. In the washed k-carrageenan gels, trapped quantum dots could be observed. Similar to CSLM, domains of dense networks could be observed, but in addition also isolated trapped particles.

# Conclusions

2D TEM showed a heterogeneous and dense networks for 0 mM NaCl κ-carrageenan gel and coarse and homogeneous networks for 50, 100, 150 and 200 mM NaCl κ-carrageenan gels. 3D TEM reconstruction of the fine network, however, was not possible due to lack of contrast.

The characterization of the biopolymer networks of κ-carrageenan gels with CLSM-FRAP was feasible and showed an immobile fraction of nanoprobes. This fraction indicates the presence of dense biopolymer networks for the κ-carrageenan gels with ≤ 100 mM NaCl. The κ-carrageenan gels prepared with 150 mM and 200 mM NaCl had a smaller immobile fraction indicating a coarse network.

The micron scale heterogeneity and homogeneity in κ-carrageenan gels was imaged using CLSM on washed gels.

TIRFM-SPT of quantum dots diffusing in k-carrageenan gels was feasible to measure. No quantification could be provided due to sub-optimal concentration of QDs.

Overall, these results shown that nanoprobes diffusometry can be used for quantitative characterization of biopolymer network heterogeneity in κ-carrageenan gels. Nanoprobe diffusometry provided even more information about the biopolymer networks of κ-carrageenan gel than TEM.

# Recommendations

The TEM contrast of the dense/fine networks can be improved by optimization of the staining method with for instance leadcitrate or uranylacetate.

The unwanted effect of bleaching during CLSM imaging in the FRAP experiment can by reduced by using less laser power during imaging and a higher concentration of nanoprobes or lowering the data point frequency. The time of the recovery in the FRAP experiment should also be increased to obtain total recovery.

For obtaining quantitative results from TIRFM-SPT experiment the concentration of the quantum dots should be between 1.7 nM and 0.3 nM.

When nanoprobe diffusometry will be applied in real-life food systems auto

fluorescence is likely to occur. This will required a carefull optimization of FRAP experiments. In case of TIRFM-SPT experiments, the influence of auto fluorescence can be reduced by using nanoprobes that emit light in the near infrared region (higher wavelengths).

# Acknowledgment

I would like to thank some people who helped me during this project. First of all I would like to thank Prof. Dr. John van Duynhoven and Dr. Johannes Hohlbein for their supervision and feedback. I also would like to thank Gerard van Dalen, Martin Koster and Caroline Romijn for their help with 3D reconstruction, CLSM and TEM within Unilever R&D Vlaardingen. Carel Fijen for teaching me to work with the TIRFM and Daan de Kort for collaboration on the κ-carrageenan gels. It has been a good learning experience, seeing both worlds of industry and academia.

# Bibliography

ATTO-TEC. (2015, december). Product information: ATTO 488. Retrieved from www.atto-tec.com: https://www.atto-tec.com/attotecshop/product_info.php?language=en&info=p99_ATTO-488.html

Axelrod, D. (2001). Total Internal Reflection Fluorescence Microscopy in Cell Biology. Traffic, 2: 764-774.

Catherine A. Konopka, S. Y. (2008). Variable-angle epifluorescence microscopy: a new way to look at protein dynamicx in the plant cell cortex. The Plant Journal , 186-196.

D. B. Williams, e. (1996). The Transmission Elctron Microscope. New York: Business Media New York.

D. de Kort, e. (2015). Nanoparticle diffusomitry for quantitative assessment of submicron structure in food biopolymer networks. Trends in Food Science & Technology, 13-26.

Davidson, T. J. (2012). Introduction to Confocal Microscopy. Retrieved 1 15, 2016, from OLYMPUS: http://olympus.magnet.fsu.edu/primer/techniques/confocal/confocalintro.html

Eils, C. K. (2004). Fluorescence recovery after photobleaching with the leica TCS SP2. German cancer research Center, Theoretical bioinformatics. Heidelberg: German Cancer Research Center.

F. van de Velde, G. d. (2012). Carrageenan. In F. v. Velde, Biopolymers (Vol. 6: polysaccarides I: polysaccharides from Eukaryotes, pp. 245-274). Weinheim: Wiley-VCH.

Hermansson, J. E. (1991). Effects of potassium, sodium and calcium on the Microsctrue and Rheological behavior of kappa-carrageenan gels. Charbohydrate polymers 16 , 297-320.

Josell, 7. (2016, February). Total internal reflection. Retrieved from Wikipedia: https://en.wikipedia.org/wiki/Total_internal_reflection#/media/File:RefractionReflextion.svg

M. B. Dürrenberger, S. H. (2001). Visualization of Food structure by Confocal Laser Scanning Microsopy (CLSM). Academic Press, 11-17.

M-L. Visnapuu, D. D. (2007). Using Total Internal Reflection Fluorescence Microsopy, DNA Curtains, and Quantum Dots to Invetigate Proetein-DNA Interactions at the Singel-molecule Level. New York: Formatex.

Morris Edwin R., R. D. (1980). Cation-specific aggregation of carrageenan helices: Domain model of polymer gel structure. J. Mol. Biol., 349-362.

Niederstrasser, H. (2015, 8 25). Electron Microscopy for dummies. Retrieved 5 24, 2014, from snaggleworks: http://www.snaggledworks.com/em_for_dummies/background.html

Tako M., n. S. (1986). Indicative evidence for a conformational trasnition in k-carrageenan from studies of viscosity-shear rate dependence. Carbohydrate Research, 200-205.

Ute Resch-Genger, M. G.-J. (2008). Quantum dots versus organic dyes as fluorescnet labels. Nature Methods, 763-775.

Vink, J. (2015). Studying interference in vivo on a single molecule scale: CRISPR on the move. Wageningen University and research center, Wageningen.

Wildenberg M. J. L., Y. j. (2010). How to Quantify Proetien Diffusion in the Baterial Membrane. Biopolymer, 312-321.

Zou, F. (2016, January). ttp://cc.scu.edu.cn. Retrieved from Techniques in Cell biology: http://cc.scu.edu.cn/G2S/Template/View.aspx

# Appendix A. Method Embedding

SOP806 Embedding in embed 812 epoxy resin

Reagents and standards

Embed 812 – after preparation storage at 4 ⁰C (maximum 6 months).

ml		or ml		or ml

DER 736	 	8 		200		400

Embed 812	 2	 	 50		100

NMA		 8.9		222.5		445

DMP 30		0.28	    	7	 	14

Glutaraldehyde (GA) 2.5% + 0.1% ruthenium red (RR) – storage 4 ⁰C

0.1 gram ruthenium red + 1 ampoule (10 ml) 25% glutaraldehyde in 100 ml demiwater

Acetone dilution range

50%, 70%, 80%, 96%, 100% in water

Method

Fixation

3 hours 2.5% GA + 0.1% RR at room temperature:

-	Bring samples (pieces of 1 mm3) in glass bottles of 10 ml

-	Add glutaraldehyde (GA) + ruthenium red (RR) solution

-	Leave in fridge for 3 hours with 2.5% GA + 0.1% RR (at room temperature)

Flush with demi-water

3x times flush with water, 20 min, 4⁰C

Dehydration

50% acetone		15min	4°C

70% acetone		15min	4°C

80% acetone		15min	4°C

96% acetone		15min	4°C

100% acetone		30min	4°C

100% acetone		30min	4°C

Impregnation (DMP-30)

Embed 812: 100% acetone = 1 : 2  		30min		room temperature

Embed 812: 100% acetone = 1 : 1  		1 hour		room temperature

Embed 812: 100% acetone = 3 : 1  		overnight	room temperature

Embed 812 				1 hour		room temperature

Embed 812 				1 hour		room temperature

Inbedding incapsules.

Hardening in oven 60°C, 24 hours (DMP-30 as hardener).

Prepare a small paper with a number, bring this number into the capsule before hardening.

Follow up

Cutting of ultrathin coupes using ultramicrotome (SOP810 Ultramicrotomy).

# Appendix B. Method Ultramicrotomy

Ultramicrotomy (SOP810)

- Syringe

- Aerosol gas ("Druckluft")

- Vacuum cleaner

- Grids

- Grids box

- Tweezers

Apparatus and equipment

- Ultramicrotome (e.g. Leica UC7)

- Diamond knife with cup

- Knife maker (e.g. Leica LKB).

- Glass rods

- Razor blades (single-edge)

- Eyelash

Procedure

Preparation

Fix the sample in Embed 812, SPURR, Lowicryl or any other resin (SOP805, SOP806, SOP812). Prepare grids with Formvar (SOP815) or order directly from supplier, with or without carbon layer.

Trim embedded sample

Embedded samples must be trimmed into a shape that is useful for sectioning: a trapezoid block face with sloping sides (a flat pyramid). The following steps should be followed:

- Tighten a sample into the sample chuck and place the chuck holder into the trimming block on the ultra-microtome stage.

- Remove excess of resin using a razor blade. Try to make the surface of the block as flat as possible.

- Prepare a trapezoid using a razor blade or glass knife.

- Cut along one side of the block at a 45-60⁰

- Rotate the block 180⁰ and repeat step 4

- Rotate the block 90⁰ and repeat step 4

- Rotate the block 180⁰ and repeat step 4.

- The final trapezoid should contain the important areas of the sample

Facing the Block

Facing the surface of the trapezoid will form a smooth, reflective surface that is required for imaging.

- Remove the trimming block and mount the knife stage on the bottom plate

- Mount the chuck holder with sample to the cutting arm of the microtome

- Place the knife holder and mount a glass knife

- Approach the knife holder until the knife is 3-4 mm from the block face

- Use the course knob to approach the sample surface. The thinner the shadow, the closer the knife edge is to the block

- Rotate the cutting wheel clockwise until a section is cut from the surface

- Start automatic cutting, e.g. at speed 50 mm/sec and feed 120 nm

- Continue until a complete trapezoid-shaped section is cut from the surface of the block

- The surface should now be flat with a mirror-like quality

Trimming with a glass knife

In some instances, it is necessary to make the sides of the trapezoid perfectly parallel and not ragged. Since this is difficult to do by hand, the top and bottom sides can be more precisely trimmed with a glass knife.

- Tilt the knife carrier so that the right edge of the upper part of the knife carrier is aligned with the 10⁰

- Slowly approach the side of the trapezoid by moving the stage forward with the course button

- Shave thin sections off the side of the trapezoid by rotating the cutting wheel

- When one side is complete, rotate the block exactly 180⁰ and repeat steps 2 and 3

Thin sectioning (50-80 nm)

The knife holder should be set back away from the sample to prevent ramming the block into the knife.

- Insert diamond knife with boat

- Use a syringe to fill the boat with filtered de-ionized water until a positive meniscus forms above the level of the boat. The boat should always be filled from the back to avoid damaging the knife edge.

- Use a syringe with a needle to withdraw water from the back of the boat until the water level is slightly below the level of the boat while still leaving the knife edge wet. The correct water level is achieved when the water near the knife edge has a uniformly silvery surface.

- Approach the knife with course and fine steps. As the knife approaches the block, a shadow of the knife edge will be projected onto the block face. The thickness of this shadow can be used to estimate the distance between the knife edge and the block face; the smaller the shadow, the closer knife edge is to the block face

- Set the cutting range (cutting rang above and below the knife edge):

    - Turn cutting wheel clockwise until block is above the knife edge

    - Press upper range button

    - Turn cutting wheel until block is below the knife edge

    - Press lower range button

- Set sectioning speed to 1.0 mm/sec. The speed may need to be varied depending on the sample.

- Set section thickness to 70 nm.

- Obtain sections thicknesses with a silver-grey interference colour.

- Go through a series of cutting strokes and remove first sections.

- Fill boat of the diamond knife until optimal height (colour of sections must be visible). The knife edge needs to be wet.

- Press green button to start sectioning automatically. A ribbon of sections should form in the boat, floating off the knife edge.

- Stop sectioning if enough sections are floating on the water.

Section Thickness

Although the ultramicrotome has a section thickness control, the true thickness of the sections should be determined from their interference colours. An interference card (below) gives a colour spectrum with the corresponding section thickness.

Collecting sections onto formvar-coated grids

There are different methods to collect sections onto grids. The first method involves plucking the sections from the surface of the water with a grid. Although this method gets the job done, it will often introduce folds on the sections. Therefore, the second method, which utilizes a perfect loop is recommended. The sections need to be supported by a thin electron-transparent film to hold the sample in place. Formvar films are a common choice of film grid. Below examples of formvar and formvar-carbon films on copper grids are shown.

- Use an eyelash to gently move the sections to the center of the boat. Do not poke the sections with the eyelash, it will damage the sections.

- Grids should be place onto filter paper inside a petri-dish (dull, bright side up) as shown in the image below.

- Hold the loop above the sections so that they appear within the center of the loop.

- Slowly lower the loop over the sections and touch the water. The sections will be held within the loop by a thin film of water.

- Lower the loop with sections onto a grid on filter paper. Wick off excess water with filter paper.

- After the loop and the grid have dried air, use an eyelash or forceps to gently separate the loop from the grid. Do not poke through the grid as this will form holes in the formvar and possibly damage the sections.

# Appendix C. 2D TEM magnification 62000 x

Fig.  30 2D TEM of 150 mM κ-carrageenan gel, representing 1.5x1.5 μm with corrections

Fig.  31 Origial 2D TEM image 0 mM κ-carrageenan gel, representing 1.5x1.7 μm

Fig.  32 2D TEM 0 mM κ-carrageenan gel, representing 1.5x1.5 μm with corrections

Fig.  33 2D TEM 50 mM κ-carrageenan gel, representing 1.5x1.5 μm with corrections

Fig.  34 2D TEM 100 mM κ-carrageenan gel, representing 1.5x1.5 μm with corrections

Fig.  35 2D TEM 200 mM κ-carrageenan gel, representing 1.5x1.5 μm with corrections

# Appendix D. FRAP data

Fig.  36 FRAP curve 0 mM NaCL carrageenan gel with dendrimer with bleach spot and reference spot.

Fig.  37 FRAP curve 50 mM NaCL carrageenan gel with dendrimer with bleach spot and reference spot.

Fig.  38 FRAP curve 100 mM NaCL carrageenan gel with dendrimer with bleach spot and reference spot

Fig.  39 FRAP curve 150 mM NaCL carrageenan gel with dendrimer with bleach spot and reference spot

Fig.  40 FRAP curve 200 mM NaCL carrageenan gel with dendrimer with bleach spot and reference spot

Fig.  41 FRAP curve free dendrimer with bleach spot and reference spot

# Appendix E. Background FRAP

Table 70. Backgrouond intensity measured six times for a 0 mM NaCL carrageenan gel and 200 mM NaCL carrageenan gel.

|  | 0 mM | 200 mM |
| --- | --- | --- |
| 1 | 1157 | 1090 |
| 2 | 1073 | 1149 |
| 3 | 1085 | 1102 |
| 4 | 1057 | 1079 |
| 5 | 1038 | 1131 |
| 6 | 1075 | 1078 |
| average | 1081 | 1105 |
| stds | 41 | 29 |
| CI 95 % | 43 | 30 |

Merging data

F-test

H0: The variation of the two groups is the same and the standard deviations can be combined

H1: The variation of the two groups is not the same and the standard deviations can’t be combined

Ftest=Ftest=sa2sb2=412292=2.00

Ftabel (probability, degrees of freedom va, degrees of freedom vb)

Ftabel (0.05; 5; 5) = 7.15

Ftest < Ftabel

H0 is accepted, the standard deviation can be combined

Sver=va*sa2+vb*sb2va+vb=5*412+5*2925+5=36

T-test

H0: The groups have the same distribution and can be merged

H1: The groups don’t have the same distribution and can’t be merged

Ttest=xa-xbsver*1na+1nb=1081-110535.5* 16+16 =1.16

Ttable (probability,degrees of freedom)

Ttable (0.05;10) = 2.23

Ttest < Ttabel

H0 is accepted, the data can be merged.

The average of the hole data set 0 mM and 200 mM can be calculted (1093)and a confedence interval can be measured

CI= t*sn= 2.23*3610 = 23

# Appendix F. Average corrected and normalized FRAP curves

Fig.  42 Average of corrected and normalized FRAP curve with standard deviation for 0 mM NaCL carrageenan gel with dendrimer.

Fig.  43 Average of corrected and normalized FRAP curve with standard deviation for 50 mM NaCL carrageenan gel with dendrimer.

Fig.  44 Average of corrected and normalized FRAP curve with standard deviation for 100 mM NaCL carrageenan gel with dendrimer.

Fig.  45 Average of corrected and normalized FRAP curve with standard deviation for 150 mM NaCL carrageenan gel with dendrimer.

Fig.  46 Average of corrected and normalized FRAP curve with standard deviation for 200 mM NaCL carrageenan gel with dendrimer.

Fig.  47 Average of corrected and normalized FRAP curve with standard deviation for dendrimer in water.

# Appendix G. CLSM images of trapped fraction

Fig.  48 Confocal image representing 1,55 x 1,55 mm of washed carrageenan gels of different sodium chloride concentration with trapped nanoprobes serie 1 top: 0 mM (left), 50 mM (middle) 100 mM (right) Bottom: 150 mM (left), 200 mM (middle), background (right)

Table 8 Measured gray values of the washed gels with different sodium chloride concentrations

| [NaCl] |  | 0 | 50 | 100 | 150 | 200 | Backgr. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Mean GRAY value | serie 1 | 17467 | 15324 | 10010 | 9538 | 8656 | 922 |
|  | serie 2 | 35608 | 24828 | 24674 | 21483 | 19311 | 921 |
| StdDEV | serie 1 | 4061 | 3049 | 2321 | 2275 | 2194 | 324 |
|  | serie 2 | 3533 | 3133 | 3005 | 2875 | 2714 | 287 |
| Mean gray value –backgr. | serie 1 | 16545 | 14402 | 9088 | 8617 | 7734 |  |
|  | serie 2 | 34687 | 23907 | 23753 | 20562 | 18390 |  |
| StdDEV | serie 1 | 3139 | 2127 | 1399 | 1353 | 1272 |  |
|  | serie 2 | 2612 | 2212 | 2084 | 1954 | 1793 |  |
| mean intensity | serie 1 | 1.00 | 0.87 | 0.55 | 0.52 | 0.47 |  |
|  | serie 2 | 1.00 | 0.69 | 0.68 | 0.59 | 0.53 |  |
| StdDEV | serie 1 | 0.19 | 0.13 | 0.08 | 0.08 | 0.08 |  |
|  | serie 2 | 0.08 | 0.06 | 0.06 | 0.06 | 0.05 |  |

# Appendix H. Plan of approach

Nanoprobe diffusion for characterization of biopolymer network

A study on kappa-carrageenan gel, using FRAP-CLSM, TRIFM and TEM

Zuidgeest, Lonneke

Plan of approach

Graduation project 			Date: 15-03-2016

Lonneke Zuidgeest 				s1078336

Unilever R&D Vlaardingen		Department Imaging & spectroscopy

Wageningen University			Laboratory of Biophysics

Hogeschool Leiden				Internship period 	01-12-2015

27-05-2016

- Graduation project, plan of approach:

- Nanoprobe diffusion for characterization of biopolymer network

Author/ student:
Name:			Lonneke Zuidgeest
Student number:	1078336
Telephone:		0611405374

Placement Company:

Name:			Wageningen University

Address:		Dreijenlaan 3

Building 312 (Transitorium)

6703 HA Wageningen

Department:		Laboratory of Biophysics

Supervisor:		Dr. Johannes Hohlbein

Email:			Johannes.hohlbein@wur.nl

Telephone:		+31-(0)317-482635

Signature supervisor:

Name:			Unilever R&D Vlaardingen

Address:		Oliver van Noortlaan 22

3133 AT Vlaardingen

Department:		Imaging & Spectroscopy

Supervisor:		Prof. Dr. John van Duynhoven

Email:			John-van.Duynhoven@unilever.com

Telephone:		+31-10-4605534

Signature supervisor:

Educational Institution:

Name:			Hogeschool Leiden

Address:		Zernikedreef 11

2333 CK Leiden

Department:		Applied Science

Study:			Chemistry

Track:	 		Analytical chemistry

Supervisor:		Pieter de Koe

Internship period:	01-12-2015 - 27-05-2016

Date:			15-03-2016

Project:

Name:			DINAMISCH

Diffusional Nanoprobes for MultI-length Scale material Characterization

Collaboration:		NWO

COAST

Unilever

Wageningen University

# Contents

Abbreviations	55

Chapter 1 Introduction	56

Chapter 2 Theory	57

2.1 Carrageenan	57

2.2 Transmission electron microscopy	58

Setup	58

Sample	59

2.3 Nanoprobes	60

2.4 CLSM-FRAP	61

Setup	62

Settings	63

FRAP data	63

2.5 TIRFM	64

Setup	64

Single particle tracking and data	65

Settings	65

Chapter 3 Planning	66

Chapter 4 Design thesis	66

Chapter 5 Bibliography	67

Appendix A. Risk assessment	68

Appendix B. SOP Embedding in Embed 812 epoxy resin	73

# Abbreviations

CLSM: 	Confocal Laser Scanning Microscopy

COAST:	Comprehensive Analytical Science and Technology

CPD:		Cumulative probability distribution

DINAMISCH:	Diffusional Nanoprobes for MultI-length Scale material Characterisation

FRAP: 		Fluorescence Recovery After Photobleaching

MSD:		Mean Square Displacement

MSDS:		Materials Safety Data Sheet

NWO:		Nederlandse Organisatie voor Wetenschappelijk Onderzoek 
Netherlands Organisation for Scientific Research

SEM:		Scanning Electron Microscopy

SPT:		Single-Particle Tracking

TEM: 		Transmission Electron Microscopy

TIRF:		Total Internal Reflection Fluorescence

# Introduction

The biopolymer network determines the morphology in food such as taste, mouthfeel, controlled release and delivery characteristics and barrier properties. The aim of this study is the characterizing and understanding of food biopolymer networks by means of electron and fluorescent microscopy. The structure of these networks consist of details on various length scales ranging from nano- to millimetres. Kappa-carrageenan gel was selected as a model system, this polysaccharide is widely used in the food industry as thickener, stabilizer and gelling agent. In presents of salt this polysaccharides forms helixes and helixes clusters in water and forms the biopolymer structure. Verifying the salt concentration influence the biopolymer network. In this study the biopolymer networks of kappa-carrageenan is first visualized with 2D and 3D transmission electron microscopy (TEM). However, this technique is invasive, potentially perturbing the network, time consuming and provides only static snapshots of the structure. To overcome these limitations, a different approach can be applied which monitors the diffusional behavior of nanoprobes in these networks to characterize and quantify structural properties. A confocal scanning laser microscope (CSLM) is used and fluorescence recovery after photobleaching (FRAP) experiments are performed with fluorescent dendrimer probes. These experiments were performed at Unilever R&D Vlaardingen. The second monitor method is single-particle tracking on a total internal reflection fluorescence microscopy (TIRFM). Quantum dots were used as nanoprobes and the experiments were done at the Wageningen University.  The trapped fraction and the diffusion coefficient of the nanoprobes were measured and verified for each of these methods. The developed methods to characterize the biopolymer structure using nanoprobes are quick, non-invasive and will improve the understanding of the biopolymer network in all sorts of food.

# Theory

## Carrageenan

Carrageenan is a polysaccharide extracted from seaweeds and specially the red algae. Carrageenan is a general name for a family of viscosifying or gel forming biopolymers. The red algea, also called Rhodophyceae uses carrageenan as cell-wall material. Since the 15th century carrageenan has been used as a thickener, stabilizer and gelling agent in mostly food. Products in which carrageenan is used are chocolate milk, (frozen) yoghurt, whipped cream, jellies, sauces and frozen desserts.  Aside in food carrageenan is also use in the pharmacy and cosmetic. Carrageenan is a biopolymer with a backbone of a mixture of sulfated D-galactose. There are three carrageenans that are most common used for food, these are identified by the Greek letter kappa (κ), lambda (λ) and iota (ι). Only kappa and iota carrageenan can form gel structure, because these polysaccharides have a 3,6-anhyrdo group. The 3,6-anhydro group are necessary to form a helix. In figure 1 the three carrageenan molecules are shown.  (F. van de Velde, 2012)

Fig. 1 Lambda, iota and kappa-carrageenan (F. van de Velde, 2012)

Κ-carrageenan gels are hard, strong and brittle gels, ι-carrageenan gels are soft and weak gel and λ-carrageenan doesn’t form a gel but is just a thickener. The gelation of kappa and iota carrageenan is due to the helics forming, which occurs by cooling hot solution of carrageenans. At a temperature of 60 °C or higher the polymer chains are in a random coil conformation, when cooling down and passing de coil-helix transition temperature the carrageenan forms helices.  The gels are thermoreversible, which means that the gels melt when heated but form again a gel when cooled. (Jordansson, 1991)

The mechanism involving the gel formation of kappa-carrageenan and the influence of salt are not well understood. Tako et al. (1985) describes the interaction of cations as intramolecular cation-selective bridge. The sulfate esters (SO3-) and 3,6-anhydro group of k-carrageenan interacted with the positive charged cation ions. The bridge is cation selective and is formed in the presences of large-site cations i.e. K+ , RB+ , Cs+, but does not form in the presence of small cations Na+ and Li+. Morris et al. (1980) found that domains were formed of “side-by-side’ helix-helix aggregations. Carrageenan gel and especially kappa-carrageenan gel needs specific cations to form this aggregations. The helix-helix aggregation is also called helices clusters, fibers, double helices, super strands or super helical rods. In the model of Morris cations form intermolecular bridges see figure 2.

Fig. 2 left: Intramolecular cation-selective brigde (Tako M., 1986), right: Intermolecular helix-helix aggregation ●: K+ ion (Morris Edwin R., 1980).

## Transmission electron microscopy

The big advantage of a transmission electron microscope (TEM) compared to a light microscope is the high resolution. Resolution in microscopy means the smallest distance between two points that can be seen. A human can see a resolution of 0,1 - 0,2 mm with their eyes, when a technique is used  to makes images with a higher resolution it’s considered to be a microscope.  Light microscopes have a resolution of approximately 300 nm. For light microscopes a higher resolution isn’t possible, because the smallest wavelength of visible light is 400 nm (violet).  For a higher resolution a smaller wavelength is necessary. Electrons can behave like a particle but also like a wave. The wavelength of the electron depends on the accelerating voltage. By increasing the accelerating voltage, the wavelength of the electrons decreases. An accelerating voltage of 100 KeV gives a resolution of 4 pm (0,004 nm). So in theory it’s possible to see atom with an electron microscope, because the resolution is lower than the diameter of an atom. However in practice this isn’t possible because of limited in lenses. A resolution of 0,1 nm is possible nowadays. (D. B. Williams, 1996)

### Setup

A TEM works like an old slide projector. A slide project has five main elements, a light source, condensing lens, a slide holder, focusing lens and a screen. A TEM has in principle the same five main elements. An electron gun is used to emit and accelerate electrons towards the sample, just like a light source. The electrons are focused using magnetic coils and lenses. Condenser and objective aperture are holes along the column of the microscope that define the size of the electron beam to change the contrast and resolution. Instead of light passing through the slide holder and projecting on the screen, electrons passing through the sample and are detected. The electrons are detected with a Cathode ray tube (CRT) detector or a sensitive camera that creates the images. The cambers of the microscope are under high vacuum, otherwise the electrons would already interact with air molecules before passing through the sample. In figure 3 left a transmission electron setup is shown and right a schematic overview. (Niederstrasser, 2015)

Fig. 3 Picture of transmission electron microscope (left), schematic overview of setup of the TEM (right). (Niederstrasser, 2015)

### Sample

There are a few requirements for the sample to get a high quality images. The specimens should be thin, otherwise all the electrons are absorbed or reflected. With a high accelerated voltage a thicker sample can be used, but the thinner the sample the better.  The best images are made with a specimen of 100 nm thick or less. Cutting thin sections can be done with an ultra-microtome. The thin sections are placed on a grid (figure 4).

Because of the high voltage the electrons have a higher energy and can damage the sample. The specious is bleached or damaged, this can be reduced by increasing the spot size. 3D images can be made with a series of images at a different angles (tomography) and conferred this series to one 3D image using special software.

The sample preparation method or the thinning processes is very time consuming and has an effect on the chemical structure of the sample. Another limitation of imaging with the TEM is that you look at a small part of your sample. So you don’t get a good overview about your whole sample. The sample preparation method is also very time consuming, that’s why (new) other methods are developed to characterize the network using nanoprobes diffusometry in this project. (D. B. Williams, 1996) (Niederstrasser, 2015)

Fig. 4 Overhead view of a grid, showing the mesh (top), side view of a carbon coated grid with sample (bottom) (Niederstrasser, 2015).

## Nanoprobes

In foods the characterization of nano structure is very important for the understanding of morphology, such a taste, mouthfeel, controlled release and delivery, water retention capacity and barrier properties. Biopolymers such as polysaccharides and proteins are forming the nanostructure networks in food. Understanding how the biopolymer strands are clustered, linked and organize will give understanding of the network on various length scales ranging from nano- to millimetres. Direct visualization is possible with transmission electron microscopy (TEM), but the sample preparation of this method are very time consuming and are likely to influence the network properties. Nanoparticle diffusion is a new analytical method in which nanoparticles are used as ‘probes’ that move through the network. The Brownian motion of the nanoparticles will scan the network. The size of the nanoparticles is very important for the diffusion in the network, too large nanoparticles will get stuck and too small nanoparticles are not influenced by the network. A nanoparticle that is a little smaller than the pores of the network, it’s not immobilized but hindered by the strands of the biopolymers and therefore characterize the network. The nanoprobes are not allowed to interact chemically with the network or stick to it. Analytical techniques that can be used to measure the diffusion of the nanoprobes are optical and fluorescence microscopy, single particle tracking and pulsed-gradient spin echo nuclear magnetic resonance (NMR). (D. de Kort, 2015)

A common used nanoparticle is a flexible polymer made of dextran, a branched polysaccharide and polyethylene glycol (PEG). In dilute solution the polymers are random coils, but in denser environment it changes in a particle. This type of particle is a dynamic particle, but there are also nanoparticles that are rigid and spherical. A broth range of rigid particles has been studied, for example proteins and solid gold colloidal nanoparticles.

Fig. 5 Dendrimer-G5-Atto

A relatively new particle is a dendrimer, a macromolecule consisting of repeating branched units. The diameter of the dendrimer are between 1 and 10 nm. For probing the biopolymer network the dendrimer has to be coated with neutral charged water soluble polymer so that it don’t stick in the network. PEG, poly vinyl alcohol (PVA), and dextran can be used for this. For the application of the nanoparticles measured with fluorescence microscopy the particles should be labeled with a fluorescent molecule, these fluorescent nanoparticles are called fluorophores. In figure 5 the fluorophore used for the FRAP experiment is showed. The dendrimer has inside an ATTO 488 dye and is coated with PEG.  (D. de Kort, 2015)

For the TIRF experiment quantum dots are used. Quantum dots are half-conducting nanocrystals. The advantages of quantum dots are their high quantum yield and Stokes shift. Quantum yield is the number of times the quantum dots emits light per absorb photon, a high quantum yield means a high efficiency. Stokes shift is the difference between the maximum excitation and maximum emission wavelength. A high Stokes shift makes it easier to detect the quantum dots. The emission of light of a quantum dot depends on their size, which is in the range of 2-20 nm in diameter. Their size can be precisely controlled during the synthesis and so a broad range of quantum dots with different emission spectrum are available. Large quantum dots emit light with a longer wavelength. Quantum dots are very bright and don’t bleach under the intense laser illumination required for TIRFM. The quantum dots are typically made from cadmium selenide (CdSe) or cadmium telluride (CdTe) with a core surrounded by ZnS shell. The naked quantum dots are only soluble in organic solvents. The semi conductive core can be coated with hydrophilic materials to make the quantum dots soluble in water.  (M-L. Visnapuu, 2007)

## CLSM-FRAP

Fluorescence recovery after photo bleaching (FRAP) experiment are widely used in research to the dynamics of molecules in living cells, membranes and other biological systems. Normally in a FRAP experiments the lipids or proteins in the sample are labeled with a fluoresced dye. For the characterizing of the biopolymer network with nanoprobes free diffusing fluorescent nanoprobes are insert in the carrageenan gel. A specific (bleach) spot is selected and the intensity of the fluorescence in this spot is measured in time.  The principle of FRAP is to photo bleach this specific spot of the sample with a short intense light pulse. The free diffusing fluorescence nanoprobes (fluorophores) in the spot are damage due to the high intensity laser pulse and the intensity of the fluorescence goes down. Directly after photo bleaching bleached fluorophores diffuse out the bleach spot and unbleached fluorophores diffuse in. This results in a recovery of the fluorescence, which is measured with a confocal laser scanning microscope (CLSM).  Using the CLSM a high resolution in a small depth of the sample can be achieved. A FRAP curve is made by plotting the intensity of fluorescence in the bleach spot in time (figure 6 right). The plot can be used to measure the fraction of mobile fluorophores and the mobility of fluorophore in the mobile phase (diffusion coefficient). See Fig. 6figure 6 for a selection of images made during the FRAP experiment with in the middle of every image the selected spot and for the FRAP curve (left).

Fig. 6 A selection of the images made during the FRAP experiment with in the middle the selected spot and image 2 the bleaching (left) and the FRAP curve (right).

6

5

4

3

1

2

### Setup

A CLSM is a fluorescently microscope that uses lasers to excited the sample and detect the fluorescence. Instead of a conventional wide field optical epi-fluorescence microscope a CLSM can produce optical sections through a three-dimensional specimen. The reason that a CLSM can obtain information from one focal plane only is the confocal pinhole placed for the detector. The pinhole is a screen with a small hole that focused only the light from the focal plane (figure 7). Optical sections in a CLSM are composed from a repeated point experiment to get a scanned image. Using CLSM for frap you can bleach very precise in a thin section.  The resolution of a CLSM is ≥0,25 μm. This is too low to measure single fluorophores with FRAP, so you look to the average diffusion of the fluorophores. (Davidson, 2012) (M. B. Dürrenberger, 2001)

Imaging in this research is done using the Leica TCS-SP5 confocal microscope with hDMI6000 inverted microscope from Unilever R&D Vlaardingen. This system is equipped with 3 lasers; an Argon laser multi-line which produces 5 lines at 458,476, 488, 496 and 514 nm, a Diode-Pumped-Solid-State (DPSS) emitting at 561 nm and a Helium-Neon laser emitting at 633 nm. Acousto-optic tuneable filters (AOTF)-controlled laser lines allow a free selection of the excitation lines and individual line alteration. The laser light is focused on the sample by a microscope objective a 10x, 40x and 63x. Fort detection, three photomultiplier tube (PMT) detectors are used, which makes scanning possible within the range of 430-750nm. The output from the PMT is built into an image.

Fig. 7 Confocal microscopy setup with laser (1), dichroic mirror (2), objective lens (3), sample (4), confocal pinhole (5), detector photomultiplier (6). (M. B. Dürrenberger, 2001)

Fig. 8 Absorption and emission (fluorescence) of Atto 488 (left), atto 488 molecuul (right) (ATTO-TEC, 2015)

### Settings

The nanonprobes are small (7 nm) and very fast diffusing. To follow the diffusion it is necessary that the CLSM makes as much as possible images (frames) per second.

Therefore the acquisition speed of the images has to be fast. A scan speed of 1400Hz line frequency and bidirectional scan is recommend to use. Bidirectional scanning means that the laser not only go from left to right but also directly back from right to left. The format from the images is responsible for the pixel size, a small format and large pixel size gives a fast scanning of the image. Because of the fast scanning the field of view must be small, so a zoom factor of 6 is required. The gain can be used to achieve more contrast and intensity. However a high gain will increase the noise, the highest signal-to-noise ratio can be achieved at a gain of 800. The bleach format is the selected spot of bleaching, the size of the bleach spot influences the diffusion. For fast diffusion a big spot is used and for slow diffusion a small spot is used. This is one of the factors that has to be optimized. The intensity of the lasers has to be high when bleaching and low for image recording. The laser power has to be optimized so that during bleaching all the fluorophores are bleached and during imaging no bleaching occurs. The fluorophore has an excitation of 450-515 nm and emission of 523 nm see figure 6. In table 1 an overview of the settings that can be used and optimized are shown.

Table 1. Setting for FRAP experiment

| Setting |  | Setting to optimize |
| --- | --- | --- |
| Objective | 10x6 | Bleach spot |
| Exciting λ | 488 nm | Intensity laser imaging |
| Detection λ | 505-605 nm | Intensity lasers bleaching |
| Gain | 800 | (Pre- /post- ) bleach time |
| Format | 512x512 | Pinhole size |
| Speed | 1400 Hz |  |
| Bidirectional | On |  |

### FRAP data

Equation 1 can be used to calculate the diffusion coefficient. It descripts the relation between the diffusion coefficient (D), the radius of the bleach spot (w) and the recovery half-time (t1/2). The half-time can be obtained from the FRAP curve by fitting an exponential function (2). F is the fluorescent intensity, a is the amplitude, t is the time, Ԏ is the time constant of recovery and c the offset. However this is an estimation of the diffusion coefficient, because this equation makes the assumptions that the bleach spot is a flat spot and diffusion occurs only in 2D. In reality the fluorophores diffuse random in all directions.  (Eils, 2004)

D=0,88*w24* t1/2                                          (1)

F=a*1-exp-tτ+c          (2)

t1/2= τ*ln2                                (3)

The validation of FRAP experiment is done by measuring the repeatability, reproducibility, detection limit. The repeatability is measured by measuring eight times the same sample and measure a 95% confidence interval. The reproducibility is done by doing the FRAP experiment on a different setup in Wageningen. The detection limit is set as the significant difference between free diffusing nanoprobes (in water) and in the gel.  The requirement for the method is that the diffusion of nanoprobes in the gels with different salt concentrations 0, 50, 100, 150 and 200 mM NaCl are significant different.

## TIRFM

Fig. 9 Light traveling from a medium with a high refraction index (n1) to a medium with a low refraction index (n2), because θ1 is bigger than θc the light is in total internal reflection (right) and an evanescent field is produced. (Josell7, 2016)

Total internal reflection fluorescence microscopy (TIRFM) uses total internal reflection between the glass and the sample to illuminate a thin layer in the sample. The small focal plane reduces the background which increases the signal to noise ratio. This is why single particles can be tracked and the diffusion coefficient can be measured with TIRFM. Total internal reflection happens when light travels from a medium with a higher reflection index to a medium with a lower reflection index for example from glass to water. If the angle of incidence is higher than the critical angle total internal reflection occurs and the light is reflected. At the same time an “evanescent field”, a thin electromagnetic field with the same frequency as the incident light is produced.  This field exponentially decease in intensity with distance from the surface, so that only the fluorophores near to the surface are excited. Snell’s law describes the relationship between the angle of incidence (θ1) and the angle of the refraction/reflection (θ2) when light traveling the interfaces of two transparent materials with different refractive index (n1 and n2). Snell’s law can also determine the critical angel (θc), this is the largest possible angle of incidence which still results in a refracted ray. The critical angle can be determined by filling in the refractive index and a refraction angle of 90 degrees (see formula 4 and figure 9). (Axelrod, 2001)	
Snell's law: Sin θ1Sin θ2=n2n1             (4)

### Setup

A home-built TIRF microscope set-up in the Laboratory of Biophysics, Wageningen will be used. This set-up uses a Lighthub® Omnicon laser engine that can independently emit laser light with four different wavelengths (404, 473, 561 and 642 nm). An ASI XY stage is built on top of a microscope objective (100x  Nikon). The angle under which the laser light is incident can be adjusted manually. The fluorescent signal can pass several bandpass filters after which the signal is split into three different channels a blue channel (480-550 nm) a green channel (570-620 nm) and a red channel (660-780 nm). The channels are split by a set of dichroic mirrors. The signal is then received by an Andor IXON-897 Ultra emCCD camera that is cooled to -80 °C. This camera records signals with a pixel size of approximately 124 nm/pixel. In figure 10 the setup is shown. (Vink, 2015)

Fig. 10 Home-built TIRFM setup laboratory of biophysical Wageningen University.

### Single particle tracking and data

Instead of images made of scanning the sample in CLSM, TIRFM makes series of wide-field images. In the images fluorescent spots are detected, localized and position-time tracks are created in Matlab software. There are two ways to obtain the diffusion coefficient from these tracks. The mean square displacement (MSD) of the particles in time and the cumulative probability distribution (CPD) function. The MSC increases linearly in time for normal diffusion and the slope is proportional for the diffusion coefficient. The diffusion of the nanoprobes in the gel are hindered by the biopolymer network so the MSD will increases in time, but the rate of increase reduces. Determining the MSD from the observed trajectories is used in many studies to analyze the tracking data op single-particles. Although this method has one disadvantage that it can’t discriminate between single particles with different diffusion coefficients and it averaged out any potential heterogeneity. The second method is to calculate the cumulative probability distribution (CPD) function of finding the particle within a circle with radius r after a given time τ. For a homogeneous population of diffusing particles, a single exponential function can be used to fit the data. A second exponential can be added for a heterogeneous population. The probability (P) that a particle starting at the origin will be found within a distance r from the origin after time τ can be given by the equation 5. (Wildenberg M. J. L., 2010)

Pr2,τ=1-exp-r24Dτ+4σ2                (5)

### Settings

Stroboscopic illumination is used, this means that the laser light illuminated for only a small time of the entire acquisition time. When continuous illumination is used for fast diffusing molecules like the quantum dots, the shape will be disturbed and a decrease in localization precision will occur. The TIRF angle has to be adjust to find the best signal to noise ratio. The most challenging is finding the right setting in the Matlab to make the position-time tracks and measure the diffusion coefficient. The software uses a tracking window to connect the quantum dot in the first image with the quantum dot which is diffused in the second image. The quantum dots are very fast diffusing this is why the tracking window should be large, but this gives the disadvantage that possibly two different quantum dots are identified as one quantum dot diffusing.  This is why the quantum dot concentration in the sample is low around 1 nM.

Table 1. Overview of setting for the TIRF microscope doing single particle tracking.

| Setting |  |  |  |
| --- | --- | --- | --- |
| Acquisition time | 10 ms | Pixel size | 124 nm |
| Illumintation time | 1 ms | Detection λ | Green channel |
| Exciting λ | 405 nm | Format | 170x255 pixels (max 512x512) |
| Intensity | 60-90% |  |  |

The same kappa-carrageenan gels as for the FRAP experiment are used. The reproducibly is tested by making 8 movies from 1000 frames and calculating a 95% confidence interval. The obtained diffusion coefficient are compared.

# Planning

| Month(s) | Planning | Location |
| --- | --- | --- |
| September/October/November | FRAP & TEM skills (2D TEM) | Unilever Vlaardingen |
| December | Optimization FRAP | Unilever Vlaardingen |
| January | TEM imaging 3D | Unilever Vlaardingen |
| February | TIRF | Wageningen |
| March | TIRF, writing | Wageningen |
| April | Deadline first version report | Wageningen |
| May | Deadline second version report | Wageningen |

| December 1 | Start graduation project Unilever Vlaardingen |
| --- | --- |
| February 1 | Start practical work Wageningen University |
| April 22 | Deadline first version report |
| May 13 | Deadline second version report |
| May 27 | End practical work |
| May 30 – June 2 | Report defense |
| June 8 | Exam day |

# Design thesis

Titel page

Summary (in Dutch and English)

Abbreviations

Table of content

Introduction

Theory

- Carrageenan

- TEM

- Nanoprobes

- FRAP

- TIRFM

- Other literature

(Materials and equipment)

Experimental Methods

- TEM

- Optimalisation FRAP

- Optimalisation TIRF

Results & Discussion

- TEM

- Optimalisation FRAP

- Optimalisation TIRF

- Comperisment different methods

Conclusion

Biography

Appendix

# Bibliography

ATTO-TEC. (2015, December). Product information: ATTO 488. Retrieved from www.atto-tec.com: https://www.atto-tec.com/attotecshop/product_info.php?language=en&info=p99_ATTO-488.html

Axelrod, D. (2001). Total Internal Reflection Fluorescence Microscopy in Cell Biology. Traffic, 2: 764-774.

D. B. Williams, e. (1996). The Transmission Elctron Microscope. New York: Business Media New York.

D. de Kort, e. (2015). Nanoparticle diffusomitry for quantitative assessment of submicron structure in food biopolymer networks. Trends in Food Science & Technology, 13-26.

Davidson, T. J. (2012). Introduction to Confocal Microscopy. Retrieved 1 15, 2016, from OLYMPUS: http://olympus.magnet.fsu.edu/primer/techniques/confocal/confocalintro.html

Eils, C. K. (2004). Fluorescence recovery after photobleaching with the leica TCS SP2. German cancer research Center, Theoretical bioinformatics. Heidelberg: German Cancer Research Center.

F. van de Velde, G. d. (2012). Carrageenan. In F. v. Velde, Biopolymers (Vol. 6: polysaccarides I: polysaccharides from Eukaryotes, pp. 245-274). Weinheim: Wiley-VCH.

Jordansson, E. E. (1991). Effects of potassium, sodium and calcium on the Microsctrue and Rheological behavior of kappa-carrageenan gels. Charbohydrate polymers 16 (, 297-320.

Josell7. (2016, February). Total internal reflection. Retrieved from Wikipedia: https://en.wikipedia.org/wiki/Total_internal_reflection#/media/File:RefractionReflextion.svg

M. B. Dürrenberger, S. H. (2001). Visualization of Food structure by Confocal Laser Scanning Microsopy (CLSM). Academic Press, 11-17.

M-L. Visnapuu, D. D. (2007). Using Total Internal Reflection Fluorescence Microsopy, DNA Curtains, and Quantum Dots to Invetigate Proetein-DNA Interactions at the Singel-molecule Level. New York: Formatex.

Morris Edwin R., R. D. (1980). Cation-specific aggregation of carrageenan helices: Domain model of polymer gel structure. J. Mol. Biol., 349-362.

Niederstrasser, H. (2015, 8 25). Electron Microscopy for dummies. Retrieved 5 24, 2014, from snaggleworks: http://www.snaggledworks.com/em_for_dummies/background.html

Tako M., n. S. (1986). Indicative evidence for a conformational trasnition in k-carrageenan from studies of viscosity-shear rate dependence. Carbohydrate Research, 200-205.

Vink, J. (2015). Studying interference in vivo on a single molecule scale: CRISPR on the move. Wageningen University and research center, Wageningen.

Wildenberg M. J. L., Y. j. (2010). How to Quantify Proetien Diffusion in the Baterial Membrane. Biopolymer, 312-321.

# Appendix A. Risk assessment

The kappa-carrageen sample used for the experiments are without any risk. The fixation and embedding of the carrageen samples is of more risk. Fixation is done with glutaraldehyde a corrosive, harmful and a potential irritant to the skin. Besides normal lab coat and glass gloves are worn. A resin embed kit is used for polymerization of the sample into a hard block. Before polymerization the embed solution is a potential dangerous. Many of the resin components are known to cause cancer in rats.

Quantum dots are quite recently developed and there potential toxicity is not fully examined. But quantum dots contain heavy metals like cadmium, which are potential risks to human health and the environment under certain condition. Safety has to be account when working with quantum dots.

The TEM has to be constantly cooled with liquid nitrogen during imaging. Liquid nitrogen has a temperature of around -200 °C and can cause cold burns in contact with skin.  The expansion ratio of nitrogen is high which means that if liquid nitrogen is rapidly vaporized in an enclosed space a large force can be generated and explode. When working with liquid nitrogen cryogenic gloves, eye and face protection are necessary.  Besides that nitrogen detectors are installed in the lab to make sure there are no leaks or to high nitrogen levels.

The laser source in the CSLM and TIRFM are potential dangers, because high intensity laser light can burn eye or even skin. The risk depends on the laser power and wavelength. The path length of the radiation of the lasers are tuned and shielded inside the microscope, so during imaging the risk is limited. Although during imaging the laser light enters the sample from below and you have to be aware to not look right in the light. When opening the microscope, be sure to turn of the lasers.

## MSDS

Acros organics

Kappa-carrageenan

| GHS Pictogram |  |
| --- | --- |
| GHS Signal Word | Warning. |
| GHS H statement | H332:; Harmful if inhales. |
| GHS P statement | P304 + P340:; IF INHALED: remove to fresh air and keep at rest in a position comfortable for breathing. |

Glutaraldehyde C5H8O2

| GHS Pictogram |  |
| --- | --- |
| GHS Signal Word | Danger. |
| GHS H statement | H290:; May be corrosive to metals. H302:; Harmful if swallowed. H334:; May cause allergy or asthma symptoms or breathing difficulties if inhaled. H315:; Causes skin irritation. H317:; May cause an allergic skin reaction. H318:; Causes serious eye damage. H335:; May cause respiratory irritation. |
| GHS P statement | P305 + P351 + P338:; IF IN EYES: Rinse cautiously with water for several minutes. Remove contact lenses, if present and easy to do. Continue rinsing. P301 + P330 + P331:; IF SWALLOWED: rinse mouth. Do NOT induce vomiting. P310:; Immediately call a POISON CENTER or doctor/physician. P261:; Avoid breathing dust/fume/gas/mist/vapors/spray. P304 + P341:; IF INHALED: If breathing is difficult, remove to fresh air and keep at rest in a position comfortable for breathing. P280:; Wear protective gloves/protective clothing/eye protection/face protection. |

Ruthenium red  Cl6 H42 N14 O2 Ru3 . 4 H2 O

| GHS Pictogram |  |
| --- | --- |
| GHS Signal Word | Warning. |
| GHS H statement | H302:; Harmful if swallowed. |
| GHS P statement | P301+ P312:; IF SWALLOWED: Call a POISON CENTER or doctor/physician if you feel unwell. |

Acetone C3H6O

| GHS Pictogram |  |
| --- | --- |
| GHS Signal Word | Danger. |
| GHS H statement | H336:; May cause drowsiness or dizziness. H319:; Causes serious eye irritation. H225:; Highly flammable liquid and vapor. EUH066:; Repeated exposure may cause skin dryness or cracking. |
| GHS P statement | P261:; Avoid breathing dust/fume/gas/mist/vapors/spray. P280:; Wear protective gloves/protective clothing/eye protection/face protection. P305 + P351 + P338:; IF IN EYES: Rinse cautiously with water for several minutes. Remove contact lenses, if present and easy to do. Continue rinsing. P210:; Keep away from heat/sparks/open flames/hot surfaces. - No smoking. P240:; Ground/Bond container and receiving equipment. |

http://www.emsdiasum.com/microscopy/technical/msds/msds.aspx

Embed 812 Resin

| GHS Pictogram |  |
| --- | --- |
| GHS Signal Word | Warning. |
| GHS H statement | H315:; Cause skin irritation. H319:; Causes serious eye irritation. H317:; May cause an allergic skin reaction. H411:; Toxic to aquatic life with long lasting effects. |
| GHS P statement | P261:; Avoid breathing dust/fume/gas/mist/vapors/spray. P280:; Wear protective gloves/protective clothing/eye protection/face protection. P305 + P351 + P338:; IF IN EYES: Rinse cautiously with water for several minutes. Remove contact lenses, if present and easy to do. Continue rinsing. P362; Take off contaminated clothing and wash before reuse. P501:; Dispose of contents/container in accordance with local/regional/national/international regulations. |

Der 736 Epoxy Resin, Polyglycoldieposides

| GHS Pictogram |  |
| --- | --- |
| GHS Signal Word | Warning. |
| GHS H statement | H302:; Harmful if swallowed. H312:; Harmful in contact with skin. H332:; Harmful if inhaled. H335:; May cause respiratory irritation. |
| GHS P statement | P261:; Avoid breathing dust/fume/gas/mist/vapors/spray. P280:; Wear protective gloves/protective clothing/eye protection/face protection. P301 + P312 +; IF SWALLOWED: call a poison center/ doctor if you feel unwell. P405; Store locked up. P501:; Dispose of contents/container in accordance with local/regional/national/international regulations. |

NMA, methyl-5-Norbornen-2,3-dicarboxylic anhydride C10H10O3

| GHS Pictogram |  |
| --- | --- |
| GHS Signal Word | Danger. |
| GHS H statement | H302:; Harmful if swallowed. H312:; Harmful in contact with skin. H319:; Causes serious eye irritation. H334:; May cause allergy or asthma symptoms or breathing difficulties if inhaled. H335:; May cause respiratory irritation. |
| GHS P statement | P261:; Avoid breathing dust/fume/gas/mist/vapors/spray. P285:; In case of inadequate ventilation wear respiratory protection. P305 + P351 + P338:; IF IN EYES: Rinse cautiously with water for several minutes. Remove contact lenses, if present and easy to do. Continue rinsing. P405; Store locked up. P501:; Dispose of contents/container in accordance with local/regional/national/international regulations. |

DMP-30 2,4,6 tris(dimethylaminomethyl)phenol C15H27N3OH

| GHS Pictogram |  |
| --- | --- |
| GHS Signal Word | Warning. |
| GHS H statement | H302:; Harmful if swallowed. H315:; Causes skin irritation. H319:; Causes serious eye irritation. |
| GHS P statement | P280:; Wear protective gloves/protective clothing/eye protection/face protection. P305 + P351 + P338:; IF IN EYES: Rinse cautiously with water for several minutes. Remove contact lenses, if present and easy to do. Continue rinsing. P301 + P312 +; IF SWALLOWED: call a poison center/ doctor if you feel unwell. P362; Take off contaminated clothing and wash before reuse. P501:; Dispose of contents/container in accordance with local/regional/national/international regulations. |

Quantum dots cd/ZnS core-shell 600 nm

| GHS Pictogram |  |
| --- | --- |
| GHS Signal Word | Danger. |
| GHS H statement | H302 + H332:; Harmful if swallowed or inhaled. H315:; Causes skin irritation. H318:; Causes serious eye damage. H350:; May cause cancer.. H373: H410:; May cause damage to organs through prolonged or repeated exposure Very toxic to aquatic life with long lasting effects. |
| GHS P statement | P201:; Obtain special intructions before use.. P261:; Avoid breathing dust/fume/gas/mist/vapors/spray. P273:; Avoid relase to the environment. P280:; Wear protective gloves/protective clothing/eye protection/face protection. P305 + P351 + P338:; IF IN EYES: Rinse cautiously with water for several minutes. Remove contact lenses, if present and easy to do. Continue rinsing. |

Sigma aldrich

# Appendix B. SOP Embedding in Embed 812 epoxy resin

Warning and safety precautions

During embedding several toxic materials are used. Always wear protection (gloves, safety glasses) and use fume hood.

Scope and field of application

This standard specifies a method for sample preparation for Transmission Electron Microscopy and can be used for different materials like cheese, tissues, dough etc. To study materials in Transmission Electron Microscopy, thin sections of samples are necessary. One of the methods to prepare a sample with a hard consistency is impregnation and embedding in a resin. The embedding in Embed 812 is useful for morphological imaging. Immunological detection of components is not possible after embedding.

Definitions

A plastic solution consists of a mixture of monomer solution, hardener, an accelerator and additional components. After hardening, the material is used to cut thin sections from the material.

Principle

To study the microstructure of soft materials using TEM, the materials can be embedded in plastic, so hard and dry material can be used. Thin coupes are cut from the resin block and gathered onto a grid.

Different steps are necessary. First fixation, then eventually block staining, followed by dehydration of the blocks with increasing acetone range. This is necessary because water doesn’t mix with Embed 812 resin. The dehydration step is followed by the impregnation step with Embed 812 (increasing concentration). After proper impregnation, the sample blocks can be embedded in small capsules with a unique number. The blocks are hardened using an oven, then samples are ready to prepare thin sections.

With Embed 812 two types of hardener can be used:

DMP-30: impregnation at room temperature and hardening at 60 ⁰C.

DMP-10: impregnation at 50 ⁰C and hardening at 70⁰C.

The advantage of use of DMP-10 as hardener is better impregnation because the resin has a lower viscosity. Disadvantage is high temperature which can influence the structure of samples.

Reagents and standards

All preparations of solutions are described in SOP: Solutions in Electron Microscopy EM (SOP804).

Embed 812 – after preparation storage at 4 ⁰C (maximum 6 months).

ml	or ml		or ml

DER 736	 8 	200		400

Embed 812	 2	  50		100

NMA		 8.9	222.5		445

DMP 30	0.28	    7		 14

Glutaraldehyde (GA) 2.5% + 0.1% ruthenium red (RR) – storage 4 ⁰C

0.1 gram ruthenium red + 1 ampoule (10 ml) 25% glutaraldehyde in 100 ml demiwater

Acetone dilution range

50%, 70%, 80%, 96%, 100% in water

Apparatus and equipment

Use standard laboratory equipment and:

Pipettes

Bottles with caps

Embed capsules 5 per sample, e.g.

BEEM Flat Embedding molds, 70904-12

BEEM 1001 capsules, size 00, 8mm ID x 20 mm high, 02305-MB

BEEM 1001B capsules, size 3, 5.6mm ID x 14 mm high, 02330-MB

SPI Silicon Embedding Mold Maroon, 7mmx14mmx5mm, 2449M-AB

Balance

Oven 60°C

Scalpel knifes

Sampling and preparation

From the samples blocks of about 1mm3 are cut with a (wet) scalpel knife. Soft samples or micro-organism can be embedded in gelatin before embed procedure.

Procedure

Safety precautions

Embedding in fume hood because toxic materials are used.

Method

For different kind of samples different procedures can be used. In this SOP a general method is described which can be used for carrageenan gels. Some other materials will need a longer procedure with more steps, this is described in appendix 1. For each material the method has to be optimized.

Fixation

3 hours 2.5% GA + 0.1% RR at 4⁰C or room temperature:

-	Bring samples (pieces of 1 mm3) in glass bottles of 10 ml

-	Add glutaraldehyde (GA) + ruthenium red (RR) solution

-	Leave in fridge for 3 hours with 2.5% GA + 0.1% RR (at 4⁰C or room temperature)

Flush with demi-water

3x times flush with water, 20 min, 4⁰C

Dehydration

50% acetone		15min	4°C

70% acetone		15min	4°C

80% acetone		15min	4°C

96% acetone		15min	4°C

100% acetone	30min	4°C

100% acetone	30min	4°C

Impregnation (DMP-30)

Embed 812: 100% acetone = 1 : 2  	30min		room temperature

Embed 812: 100% acetone = 1 : 1  	1 hour		room temperature

Embed 812: 100% acetone = 3 : 1  	overnight	room temperature

Embed 812 				1 hour		room temperature

Embed 812 				1 hour		room temperature

Inbedding incapsules.

Hardening in oven 60°C, 24 hours (DMP-30 as hardener).

Prepare a small paper with a number, bring this number into the capsule before hardening.

Follow up

Cutting of ultrathin coupes using ultramicrotome (SOP810 Ultramicrotomy).

Quality assurance and control

The method is kept under control by analyzing a control sample (if available) with every batch of samples. This is a sample with a known micro structure.